# SECTION 09440

# EPOXY MATRIX TERRAZZO

# Dex-O-Tex Cheminert Terrazzo

# PART 1.00 - GENERAL

# 1.01	GENERAL REQUIREMENTS

A.	Work of this Section, as shown or specified, shall be in accordance with the requirements of the Contract Documents.

# 1.02	WORK INCLUDED

A.	Work of this Section includes all labor, materials, equipment and services necessary to complete epoxy matrix terrazzo flooring and integral coved base as selected on drawings and/or specified herein.

# 1.03	RELATED WORK

A.	Concrete - Section 03300 (Note to specifier:  Concrete should be either water cured or cured using curing compounds  in compliance with ASTM C309 or ASTM C1315 only.  Other types of curing compounds are generally not acceptable.  Concrete should be cured for a minimum of 28 days and exhibit a MVER of 3lbs/24 hrs/1000SF.  On grade floors should have functioning vapor retarder beneath slab.)

B.	Floor drains - Division 15.  (Note to Specifier:  Floor drains, clean-outs, etc. should be of the floor-flange type as manufactured for use with composition floors by most major drain manufacturers.)

# 1.04	SUBMITTALS

A.	General:  Submit the following in accordance with Conditions of Contract and Division 1 Specification Sections.

B.	Product Data:  Submit manufacturer's technical data, application instructions and general recommendations for epoxy matrix terrazzo flooring specified herein.

C.	LEED Submittals:

1.  	Product Data for Credit MR 4.1 and Credit MR 4.2:  For products having recycled content, submit documentation indicating percentages by weight of postconsumer and preconsumer recycled content.

a.   	Include statement indicating costs for each product having recycled content.

b.	Include LEED Product Information Form for LEED Credits MR 4.1 and 4.2.

2.	Product Data for Credit EQ 4.2:  For field applied, interior, paints coatings and primers, include printed statement of VOC content indicating compliance with Credit requirements.

a.	Include LEED Product Information Form for LEED Credit EQ 4.2.

3.	Provide additional documentation for products as required to achieve each Credit(s).

D.	Samples for initial selection purposes.

1.  Submit 2-1/2" x 4" samples in color combination as selected.

E.	Material certificates signed by manufacturer certifying that epoxy matrix terrazzo flooring        comply with requirements specified herein.

F.	Maintenance Instructions:  Submit manufacturer's written instructions for recommended maintenance practices.

# 1.05	QUALITY ASSURANCE

A.	Installer Qualifications:  Engage an experienced installer or applicator who has specialized in     installing resinous terrazzo flooring similar to that required for this Project and who is acceptable to manufacturer of primary materials.

B.	Single-Source Responsibility:  Obtain epoxy matrix component of terrazzo flooring materials, including primers, resins, hardening agents, and finish or sealing coats, from a single manufacturer.  Obtain marble chip aggregates and metal dividing strips from primary manufacturers of those products.

C.	Contractor Job Site Log: Contractor shall document daily; the work accomplished, environmental conditions and any other condition or event significant to the long term performance of the terrazzo installation. The contractor shall maintain these records for one year after substantial completion

# 1.06	DELIVERY STORAGE AND HANDLING

A.	Deliver materials in original packages and containers with seals unbroken and bearing manufacturer's labels containing brand name and directions for storage and mixing with other components.

B.	Store materials to comply with manufacturer's directions to prevent deterioration from moisture, heat, cold, direct sunlight, or other detrimental effects.

# 1.07	PROJECT CONDITIONS

A.	Environmental Conditions:  Comply with epoxy matrix terrazzo manufacturer's directions for maintenance of ambient and substrate temperature, moisture, humidity, ventilation, and other conditions required to execute and protect work.

B.	Lighting:  Permanent lighting will be in place and working before installing epoxy matrix terrazzo flooring.

# PART 2:00 - PRODUCTS

# 2.01	 MATERIALS

A.	Epoxy matrix terrazzo shall be Dex-O-Tex Cheminert Terrazzo as manufactured by Crossfield Products Corp. in Rancho Dominguez, California and Roselle Park, New Jersey.

# 2.02	PROPERTIES

A.	Colors:  As indicated, or if not otherwise indicated, as selected by Architect from manufacturer's standard matrix colors with marble chips as regionally available.

B.	Physical Properties:  Provide flooring system that meets or exceeds the listed minimum physical property requirements using specified epoxy matrix incorporating marble aggregate as per manufacturer's mix recommendations when tested according to the referenced standard test method in parentheses.

Compressive Strength (ASTM D695)	12,000 psi

Impact Resistance (MIL-PRF-3134 Para 4.7.3)	0.005" indentation,

no loosening or cracking

Indentation Resistance (MIL-PRF-3134, Para. 4.7.4.2.1)	No Indentation

Adhesion (A.C.I. Committee 503.1)	>525 psi.

100% failure in concrete

Resistance to Elevated Temperatures	No slip, flow or softening

(MIL-PRF-3134 Para. 4.7.5.1)

Co-efficient of Linear Expansion (ASTM D696)	14 x 106 (max.) per degree F/120

F to 1400 F

Tensile Strength (ASTM C638)	3,400 psi.

Flammability (FTMS 372/NFPA 253/ ASTM E648)	Greater than 1.07 watts/cm

# 2.03	SUPPLEMENTAL MATERIALS

A.	Waterproofing Membrane:  Type recommended or produced by manufacturer of epoxy resin composition flooring system for type of service and floor condition indicated.  (Note to Specifier:  The use of waterproof membrane is optional and is generally confined to suspended floors and in rooms having floor drains and subject to very wet spillage and service.  All areas requiring membrane treatment should be clearly shown on plans and finish schedules.)

B.	Anti-Microbial Additive:  Incorporate antimicrobial chemical additive to prevent growth of most bacteria, fungi, algae and actinomycetes.  (Note to Specifier:  The use of antimicrobial additive is optional.  Does not poses any health hazard.)

C.	Dividing Strips:  Type as manufactured for use with thin-set epoxy matrix terrazzo (Note to Specifier:  Typical dividing strip is white alloy of zinc in gauge 18, 16 or 14).

# PART 3.00 - EXECUTION

# 3.01	INSPECTION

A.	Examine the areas and conditions where epoxy matrix terrazzo flooring is to be installed and notify the Architect of conditions detrimental to the proper and timely completion of the work.

Do not proceed with the work until unsatisfactory conditions have been corrected by the Contractor in a manner acceptable to the Architect.

B	Moisture Vapor Transmission Test. Perform calcium chloride moisture vapor transmission test to accurately evaluate the volume of moisture being emitted from the concrete substrate. Provide a written report showing the test placement and results. Do not proceed if the MVT rate is higher than that recommended by the manufacturer until such conditions are correct to the satisfaction of the architect. (Note to Specifier: the MVT threshold for the Dex-O-Tex Systems recommended in this specification is 3 lbs per/ 1000 Square Feet/ 24 hour period. When the MVT emission exceeds this limit, use Dex-O-Tex VaporControl Primer 200 or 100 prior to application of the flooring or membrane systems.)

# 3.02	PREPARATION

A.	Substrate:  Perform preparation and cleaning procedures according to flooring manufacturer's instructions for particular substrate conditions involved and as specified.  Provide clean, dry and neutral substrate for flooring application.

B.	Concrete Surfaces:  Shot-blast, acid etch or power scarify as required to obtain optimum bond of flooring to concrete.  Remove sufficient material to provide a sound surface free of laitance, glaze, efflorescence and any bond-inhibiting curing compounds or form release agents.  Remove grease, oil and other penetrating contaminates.  Repair damaged and deteriorated       concrete to acceptable condition.  Leave surface free of dust, dirt, laitance and efflorescence.

C.	Materials:  Mix epoxy matrix flooring components when required and prepare materials according to flooring system manufacturer's instructions.

# 3.03	APPLICATION

A.	General:  Apply each component of epoxy matrix terrazzo flooring system according to manufacturer's directions to produce a uniform monolithic flooring surface of thickness indicated.

B.	Bond Coat:  Apply epoxy bond coat over prepared substrate at manufacturer's recommended spreading rate.

C.	Divider Strips:  Set divider strips as indicated on plans. Strips shall be set in a full bed of epoxy adhesive and allowed to cure before proceeding with the work.

D.	Body Coat:  Over bond coat surface trowel apply epoxy matrix terrazzo to thickness of ___.     (Note to Specifier:  Epoxy matrix terrazzo is typically applied in either 1/4" or 3/8" thickness. Specification of 3/8" thickness provides floor which helps fair off undulations in concrete surfaces). Seed the surface with additional aggregate of the same blend as the trowel applied mortar. Work the aggregate into the surface to an even aggregate chip dispersion. Compact the matrix into a tight even compound.

E.	Grinding:  Grind floor using terrazzo grinding machines, mounting progressively finer grit stones to achieve flat surface with uniform exposure of marble chips.

F.	Grouting and Finish Grind:  Grout floor with epoxy resin and finish grind to remove grout.

G.	Sealing Coats:  Apply sealing coats of type recommended by manufacturer to produce finish matching approved samples.  Finished floor shall be ___ thick   (Note to specifier: Indicate desired thickness).

# 3.04	CURING, PROTECTION AND CLEANING

A.	Cure epoxy matrix terrazzo flooring materials according to manufacturer's directions, taking care to prevent contamination during application stages and before completing curing process.  Close application area for a minimum of 24 hours.

# END OF SECTION

DEX-O-TEX PRODUCT LINE			3000 E. Harcourt Street		140 Valley Road

Crossfield Products Corp.			Rancho Dominguez, CA 90221		Roselle Park, NJ 07204

www.dexotex.com				Tel: (310) 886-9100			Tel: (908) 245-2800

Fax: (310) 886-9119			Fax: (908) 245-2583