SECTION 09830

FLEXIBILIZED URETHANE EPOXY RESIN WATERPROOF MEMBRANE

Dex-O-Tex Flex-Shield

PART 1.00 - GENERAL

1.01	GENERAL REQUIREMENTS

A.	Work of this Section, as shown or specified, shall be in accordance with the requirements of the Contract Documents.

1.02	WORK INCLUDED

A.	Work of this Section includes all labor, materials, equipment and services necessary to complete the flexibilized urethane epoxy specialty flooring system as scheduled on the drawings and/or specified herein.

1.03	RELATED WORK

A.	Concrete - Section 03300.

(Note to Specifier:  Concrete should be either water cured or in accordance with ASTM C159 or ASTM C309.  Other types of curing compounds are generally not acceptable.  Concrete should be cured for a minimum of 28 days.  On grade floors should have functioning vapor retarder beneath slab.)

B.	Floor drains - Division 15.

(Note to Specifier:  Floor drains, clean-outs, etc. should be of the "floor-flange" type as manufactured for use with composition floors by most major drain manufacturers.)

1.04	SUBMITTALS

A.	General:  Submit the following in accordance with Conditions of Contract and Division 1 Specification Sections.

B.	Product Data:  Submit manufacturer's technical data, application instructions and general recommendations for the flexibilized urethane epoxy specialty flooring system specified herein.

C.	LEED Submittals:

1.  	Product Data for Credit MR 4.1 and Credit MR 4.2:  For products having recycled content, submit documentation indicating percentages by weight of postconsumer and preconsumer recycled content.

a.   	Include statement indicating costs for each product having recycled content.

b.	Include LEED Product Information Form for LEED Credits MR 4.1 and 4.2.

2.	Product Data for Credit EQ 4.2:  For field applied, interior, paints coatings and primers, include printed statement of VOC content indicating compliance with Credit requirements.

a.	Include LEED Product Information Form for LEED Credit EQ 4.2.

3.	Provide additional documentation for products as required to achieve each Credit(s).

D.	Samples for initial selection purposes in form of manufacturer's color charts showing full range of colors and finishes available.

E.	Submit 2-1/2" x 4" samples of color chips from color chart selection designated by the Architect.

- Provide 12” X 12” Mock-up samples made by the installing contractor in the color, texture and final finish. Approved mock up samples will be used as the standard for quality of the application

F.	Material certificates signed by manufacturer certifying that the flexibilized urethane epoxy resin specialty flooring system complies with requirements specified herein.

G.	Submit a letter from the primary manufacturer of the materials used, that the contractor is acceptable to the materials manufacturer and that the materials manufacturer will jointly guarantee the application with the installing contractor

H.	Maintenance Instructions:  Submit manufacturer's written instructions for recommended maintenance practices.

1.05	QUALITY ASSURANCE

A.	Installer Qualifications: Engage an experienced Installer or applicator who has specialized in installing resinous flooring types similar to that required for this Project the Installer shall provide a letter from the manufacturer stating that the installer is a qualified applicator of flexibilized urethane epoxy resin flooring system. Additionally the installer shall submit with their proposal, five references of similar applications including contact names and phone numbers for verification.

B.	Single-Source Responsibility:  Obtain flexibilized urethane epoxy resin flooring system materials, including primers, resins, hardening agents, and finish or sealing coats, from a single manufacturer.

C.	Qualified Materials: Request for material approvals for any products other than the specified products must be submitted to the Architect two weeks prior to the bid, including complete application specification, physical characteristics, and chemical resistance data. Any request after this date will not be accepted. Failure of performance requires immediate removal and replacement of unapproved substituted material with those originally specified at no cost to the owner, Architect, construction manager, or general contractor.

1.06	DELIVERY, STORAGE AND HANDLING

A.	Deliver materials in original packages and containers with seals unbroken and bearing manufacturer's labels containing brand name and directions for storage and mixing with other components.

B.	Store materials to comply with manufacturer's directions to prevent deterioration from moisture, heat, cold, direct sunlight, or other detrimental effects.

1.07	PROJECT CONDITIONS

A.	Environmental Conditions:  Comply with flexibilized urethane epoxy specialty flooring system manufacturer's directions for maintenance of ambient and substrate temperature, moisture, humidity, ventilation, and other conditions required to execute and protect Work.

B.	Lighting:  Permanent lighting will be in place and working before installing resinous flooring.

PART 2.00 - PRODUCTS

2.01	MATERIALS

A.	Troweled flexibilized urethane epoxy specialty flooring system shall be Dex-O-Tex Flex-Shield as manufactured by Crossfield Products Corp., Rancho Dominguez, California; Roselle Park, New Jersey.

2.02	PROPERTIES

A.	Colors:  As indicated, or if not otherwise indicated, as selected by Architect from manufacturer's standard colors.

B.	Physical Properties: Provide flooring system that meets or exceeds the listed minimum physical property requirements when tested according to the referenced standard test method in parentheses.

Tensile Strength (ASTM C307)				1,500 psi

Tensile Modulas					17,150 psi

Tensile Elongation					96%

Tear Strength						120 lb./in.

Bond Strength ACI #403					400 psi

(100% concrete failure)

Surface Hardness (ASTM D2240)		                              55 Shore D

Chemical Resistance (ASTM D1308)

Gasoline					No Effect

Kerosene				No Effect

Skydrol 					No Effect

Isopropyl Alcohol			No Effect

Toluene					No Effect

Hydrogen Peroxide			Slight Stain

Hydrochloric Acid (25%)       		    No Effect

2.03	SUPPLEMENTAL MATERIALS

A.	Finish coat:  Type recommended for specific project requirements and produced by manufacturer of flexibilized urethane epoxy specialty flooring system.

Note to Specifier:  Standard finish coat for the Flex-Shield system is an aliphatic poly-urea which offers good flexibility, UV resistance and chemical resistance.  Other finish coats are available meet specific requirements for specialized applications.  Consult manufacturer for recommended type).

PART 3.00 - EXECUTION

3.01	INSPECTION

A.	Examine the areas and conditions where the flexibilized urethane epoxy specialty flooring system is to be installed and notify the Architect of conditions detrimental to the proper and timely completion of the work.  Do not proceed with the work until unsatisfactory conditions have been corrected by the Contractor in a manner acceptable to the Architect.

B.	Evaluate level of moisture in the substrate in compliance with ASTM F1869 or ASTM F2170 to determine if the moisture levels are acceptable for application of specified flooring system. Submit report to the Project Supervisor and Architect detailing the results of the MVT test.

3.02   	PREPARATION

A.	Substrate:  Perform preparation and cleaning procedures according with SSPC-SP 13 and flooring manufacturer's instructions for particular substrate conditions involved, as specified.  Provide clean, dry, and neutral substrate for flooring application.

B.	Concrete Surfaces:  Shot-blast, or power scarify as required to obtain optimum bond of flooring to concrete.  Remove sufficient material to provide a sound surface free of laitance, glaze, efflorescence, and any bond-inhibiting curing compounds or form release agents.  Remove grease, oil, and other penetrating contaminates.  Repair damaged and deteriorated concrete to acceptable condition.  Leave surface free of dust, dirt, laitance, and efflorescence.

C.	Materials:  Mix resin hardener and aggregate when required, and prepare materials according to flooring system manufacturer's instructions.

3.03	APPLICATION

A.	General:  Apply each component of flexibilized urethane epoxy specialty flooring system according to manufacturer's directions to produce a uniform monolithic flooring surface of thickness indicated.

B.	Bond Coat:  Apply bond coat over prepared substrate at manufacturer's recommended spreading rate.

C.	Body Coat:  Over primer, trowel apply flexibilized urethane epoxy mix at nominal 5/64-inch (77 mils) thickness. Broadcast appropriate aggregates into the wet base coat to an even and uniform surface profile.

D.	Finish Coat:  apply top coat finish coating as selected over cured and prepared body coat. Apply finish coat in two successive applications. Provide a uniform even final finish.

1.	Final finish coat shall be in color and skid retardant profile as approved by the Architect.

2.	Finished floor shall be 1/8" thick, uniform in color and free of trowel marks.

E.	Cove Base:  Apply cove base mix to wall surfaces at locations shown to form cove base height of 4 inches unless otherwise indicated.  Follow manufacturer's printed instructions and details including taping, mixing, priming, troweling, sanding, and top-coating of cove base.

- CURING, PROTECTION AND CLEANING

- Cure flexibilized urethane epoxy specialty flooring system materials according to manufacturer's directions, taking care to prevent contamination during application stages and before completing curing process.  Close application area for a minimum of 24 hours.

END OF SECTION