# SECTION 09810

# SLIP-RETARDENT EPOXY FLOOR COATING

# Dex-O-Tex Posi-Tred “CR”

# PART 1.00 - GENERAL

# 1.01	GENERAL REQUIREMENTS

A.	Work of this Section, as shown or specified, shall be in accordance with the requirements of the Contract 	Documents.

# 1.02	WORK INCLUDED

A.	Work of this Section includes all labor, materials, equipment and services necessary to complete slip-                     	 retardant epoxy floor coating as selected on drawings and/or specified herein.

# 1.03	RELATED WORK

A.	Concrete - Section 03300

(Note to Specifier: Concrete should be either water cured or cured using sodium silicate curing 		compounds only.  Other types of curing compounds are generally not acceptable.  Concrete should 	be cured for a minimum of 28 days.  On grade floors should have functioning vapor retarder 	beneath slab.)

# 1.04	SUBMITTALS

A.	General: Submit the following in accordance with Conditions of Contract and Division 1 Specification                    	Sections.

B.	Product Data: Submit manufacturer’s technical data, application instructions and general 	recommendations for slip-retardant epoxy coating floor coating specified herein.

C.	LEED Submittals:

1.  	Product Data for Credit MR 4.1 and Credit MR 4.2:  For products having recycled content, submit documentation indicating percentages by weight of postconsumer and preconsumer recycled content.

a.   	Include statement indicating costs for each product having recycled content.

b.	Include LEED Product Information Form for LEED Credits MR 4.1 and 4.2.

2.	Product Data for Credit EQ 4.2:  For field applied, interior, paints coatings and primers, include printed statement of VOC content indicating compliance with Credit requirements.

a.	Include LEED Product Information Form for LEED Credit EQ 4.2.

3.	Provide additional documentation for products as required to achieve each Credit(s).

D.	Samples:

1) Submit 2-1/1” x 4” samples in color and profile as selected.

E.	Material certificates signed by manufacturer certifying that the slip-retardant epoxy coating floor coating 	complies with requirements specified herein.

F.	Maintenance Instructions: Submit manufacturer’s written instructions for recommended maintenance                    	 practices.

# 1.05	QUALITY ASSURANCE

A.	Installer Qualifications: Engage an experienced Installer or applicator who has specialized in installing                   	resinous flooring types similar to that required for this Project and who is acceptable to manufacturer of                 	 primary materials.

B.	Single-Source Responsibility: Obtain epoxy floor coating materials including primers, slip-retardant                       	aggregates, resins, hardening agents and finish coats from a single manufacturer.

# 1.06	DELIVERY STORAGE AND HANDLING

A.	Deliver materials in original packages and containers with seals unbroken and bearing manufacturer’s 	labels containing brand name and directions for storage and mixing with other components.

B.	Store materials to comply with manufacturer’s directions to prevent deterioration from moisture, heat, 	cold, direct sunlight, or other detrimental effects.

# 1.07	PROJECT CONDITIONS

A.	Environmental Conditions: Comply with slip-retardant epoxy coating manufacturer’s directions for                         	maintenance of ambient and substrate temperature, moisture, humidity, ventilation, and other conditions               	 required to execute and protect work.

B.	Lighting: Permanent lighting will be in place and working before installing epoxy floor coating.

# PART 2.00 - PRODUCTS

# 2.01	MATERIALS

A.	Slip-retardant epoxy coating shall be Dex-O-Tex Posi-Tred “O” as manufactured by Crossfield Products                 Corp. in Rancho Dominguez, California and Roselle Park, New Jersey.

# 2.02	PROPERTIES

A.	Colors: As indicated, or if not otherwise indicated, as selected by Architect from manufacturer’s standard                colors which must include white and off-white.

B.	Physical Properties: Provide floor coating system that meets or exceeds the listed minimum physical                        property requirements when tested according to the referenced standard test method in parentheses.

# Overall Thickness (Dry Film) to Top of Slip-Retardant Aggregate:

Very Fine Profile 		3 mils

Fine Profile			18 mils

Medium Profile			32 mils

Coarse Profile			54 mils

Very Coarse Profile		90 mils

# Coefficient of Friction-Rubber Shoe Surface: (MIL-PRF-3134 Test Procedure):

# Static Friction:

Saltwater Solution on Surface	Oil on Surface

Fine Profile			0.95				0.75

Medium Profile			1.03				0.75

Coarse Profile			1.09				0.85

Very Coarse Profile		1.24				0.78

# Sliding Friction:

Saltwater Solution on Surface	Oil on Surface

Fine Profile			0.89				0.44

Medium Profile			0.95				0.45

Coarse Profile			1.00				0.56

Very Coarse Profile		1.04				0.59

# Chemical Resistance:

ASTM D-1308				(Total Immersion – 7 days)

Citric Acid (70%)			No Effect

Hydrochloric Acid (46%)			No Effect

Sulfuric Acid (96%)			No Effect

Sodium Hydroxide (50%)			No Effect

Lactic Acid				No Effect

Methyl Ethyl Ketone			No Effect

Hydraulic Fluid				No Effect

Butyl Acetate				No Effect

# Resistance to Immersion:

MIL-PRF-23003A Para. 4.6.11		No softening, loss of adhesion or

SAE 10 Oil 				other form of deterioration

Detergent Solution

# Fire Resistance:				Flame Spread Index - 0

ASTM E162				Smoke Deposited - 2mg

# PART 3.00 - EXECUTION

# 3.01	INSPECTION

A.	Examine the areas and conditions where slip-retardant epoxy floor coating is to be installed and notify the 	Architect of conditions detrimental to the proper and timely completion of the work.  Do not proceed with               	the work until unsatisfactory conditions have been corrected by the Contractor in a manner acceptable to                	 the Architect.

# 3.02	PREPARATION

A.	Substrate: Perform preparation and cleaning procedures according to flooring manufacturer’s instructions              	 for particular substrate conditions involved, and as specified.  Provide clean, dry, and neutral substrate for               flooring application.

B.	Concrete Surfaces: Shot-blast, acid etch or power scarify as required to obtain optimum bond of flooring 	to concrete.  Remove sufficient material to provide a sound surface free laitance, glaze, efflorescence, and 	any bond-inhibiting curing compounds or form release agents.  Remove grease, oil, and other penetrating 		contaminates.  Repair damaged and deteriorated concrete to acceptable condition.  Leave surface free of                 	 dust, dirt, laitance, and efflorescence.

C.	Materials: Mix epoxy primer and urethane coating components when required and prepare materials                       	according to manufacturer’s instructions.

# 3.03	APPLICATION

A.	General: Apply each component of slip-retardant epoxy coating service floor coating system according to 	manufacturer’s directions to produce a uniform monolithic flooring surface.

- Bond Coat: Apply epoxy bond coat over prepared substrate at manufacturer’s recommended spreading rate by roller, squeegee, trowel or spray.

- Basecoat: Trowel, roller or squeegee apply two or three coats of Posi-Tred CR as required with appropriate skid resistant profile.

# 3.04	CURING, PROTECTION AND CLEANING

A.	Cure epoxy floor coating materials according to manufacturer’s directions, taking care to prevent                           	 contamination during application stages and before completing curing process.  Close application area for 	a minimum of 24 hours.

# END OF SECTION

DEX-O-TEX PRODUCT LINE			3000 E. Harcourt Street		140 Valley Road

Crossfield Products Corp.			Rancho Dominguez, CA 90221		Roselle Park, NJ 07204

www.dexotex.com				Tel: (310) 886-9100			Tel: (908) 245-2800

Fax: (310) 886-9119			Fax: (908) 245-2583