SECTION 09851

EPOXY CHEMICAL RESISTANT WALL COATING

Dex-O-Tex Wallcote “W”

## PART 1.00 – GENERAL

1.01	GENERAL REQUIREMENTS

A.	Work of this Section, as shown or specified, shall be in accordance with the requirements of the Contract Documents.

1.02	WORK INCLUDED

A.	Work of this Section includes all labor, materials, equipment and services necessary to complete epoxy resin chemical resistant wall coating as shown on drawings and/or specified herein.

1.03	RELATED WORK

- Gypsum Board – Section 09250.

1.04	SUBMITTALS

A.	General:  Submit the following in accordance with Conditions of Contract and Division 1 Specification Sections.

B.	Product Data:  Submit manufacturer's technical data, application instructions and general recommendations for epoxy resin chemical resistant wall coating specified herein.

C.	LEED Submittals:

1.  	Product Data for Credit MR 4.1 and Credit MR 4.2:  For products having recycled content, submit documentation indicating percentages by weight of postconsumer and preconsumer recycled content.

a.   	Include statement indicating costs for each product having recycled content.

b.	Include LEED Product Information Form for LEED Credits MR 4.1 and 4.2.

2.	Product Data for Credit EQ 4.2:  For field applied, interior, paints coatings and primers, include printed statement of VOC content indicating compliance with Credit requirements.

a.	Include LEED Product Information Form for LEED Credit EQ 4.2.

3.	Provide additional documentation for products as required to achieve each Credit(s).

D.	Samples for initial selection purposes in form of manufacturer's color charts showing full range of colors and finishes available.

- Submit 2-1/2" x 4" sample in color as selected.

E.	Material certificates signed by manufacturer certifying that the epoxy resin chemical resistant wall coating complies with requirements specified herein and is 100% non-volatile epoxy solids exhibiting no odor at no time of application.

F.	Maintenance Instructions:  Submit manufacturer's written instructions for recommended maintenance practices.

1.05	QUALITY ASSURANCE

A.	Installer Qualifications:  Engage an experienced Installer or applicator who has specialized in installing resinous flooring types similar to that required for this Project and who is acceptable to manufacturer of primary materials.

B.	Single-Source Responsibility:  Obtain epoxy resin chemical resistant wall coating materials, including primers, resins, hardening agents, and finish or sealing coats, from a single manufacturer.

1.06	DELIVERY, STORAGE AND HANDLING

A.	Deliver materials in original packages and containers with seals unbroken and bearing manufacturer's labels containing brand name and directions for storage and mixing with other components.

B.	Store materials to comply with manufacturer's directions to prevent deterioration from moisture, heat, cold, direct sunlight, or other detrimental effects.

1.07	PROJECT CONDITIONS

A.	Environmental Conditions: Comply with epoxy resin chemical resistant wall coating manufacturer's directions for maintenance of ambient and substrate temperature, moisture, humidity, ventilation, and other conditions required to execute and protect Work.

B.	Lighting: Permanent lighting will be in place and working before installing wall coating.

## PART 2.00 – PRODUCTS

2.01	MATERIALS

A.	Epoxy resin chemical resistant wall coating shall be Dex-O-Tex Wallcote “W” as manufactured by Crossfield Products Corp. in Rancho Dominguez, California and Roselle Park, New Jersey.

2.02	PROPERTIES

A.	Colors:  As indicated, or if not otherwise indicated, as selected by Architect from manufacturer's standard colors.

B.	Physical Properties: Provide wall coating that meets or exceeds the listed minimum physical property requirements when tested according to the referenced standard test method in parentheses.

Solids Content	100% epoxy solids

Thickness	11 mils

Compressive Strength (ASTM D695)	8,000 psi.

Odor at Installation	Nil

Elongation (ASTM D638)	13%

Surface Hardness (ASTM D2240)	Scale: D: 62

Adhesion (ASTM D695)	Exceeds internal strength of gypsum

Board backing

Volatile Organic Content	None

Flexibility (ASTM D522)	Passes 1/8” mandrel at 180º bend

Without cracking

Wear Resistance (ASTM D1044)	16mg. Weight loss

Water Absorption (MIL-PRF-3134, Para. 4.7.8)	<0.5% psi

Cleanability (TT-C-550a)	Complies

Flash Point (Tag Closed Cup)	Exceeds 200ºF.

2.03	SUPPLEMENTAL MATERIALS

A.	Anti-Microbial Additive: Incorporate anti-microbial chemical additive to prevent growth of most bacteria, fungi, algae and actinomycetes. (Note to Specifier:  The use of anti-microbial additive is optional. Its use poses no health hazard.)

PART 3.00 - EXECUTION

3.01	INSPECTION

A.	Examine the areas and conditions where epoxy resin chemical resistant wall coating is to be installed and notify the Architect of conditions detrimental to the proper and timely completion of the work including absence of adjacent floor bases or other construction elements which are to be overlapped by wall coating. Do not proceed with the work until unsatisfactory conditions have been corrected by the Contractor in a manner acceptable to the Architect.

3.02   	PREPARATION

A.	Substrate:  Perform preparation and cleaning procedures according to flooring manufacturer's instructions for particular substrate conditions involved, and as specified. Provide clean, dry, substrate.

B.	Materials:  Mix epoxy resin components when required, and prepare materials according to wall coating system manufacturer's instructions.

3.03	APPLICATION

A.	General:  Apply each component epoxy resin chemical resistant wall coating system according to manufacturer's directions to produce a uniform monolithic wall coating of thickness indicated.

B.	Bond Coat:  Apply bond coat over prepared substrate at manufacturer's recommended spreading rate.

- Body Coat:  Over bond coat apply epoxy resin chemical resistant wall coating.  Overlay adjacent floor base, door frames, etc. as shown on plans.

- Finish or Sealing Coats: After body coat has cured sufficiently, apply epoxy resin finish coat to produce finish matching approved sample and in number of coats and spreading rates recommended by manufacturer.

- Final finish coat shall be in color as approved by the Architect.

- Finished wall coating shall be 11 mils thick, uniform in color and texture.

    - CURING, PROTECTION AND CLEANING

- Cure epoxy resin chemical resistant wall coating materials according to manufacturer's directions, taking care to prevent contamination during application stages and before completing curing process.  Close application area for a minimum of 24 hours.

# END OF SECTION

DEX-O-TEX PRODUCT LINE 			3000 E. Harcourt Street		140 Valley Road

Crossfield Products Corp.			Rancho Dominguez, CA 90221		Roselle Park, NJ 07204

www.dexotex.com				Tel: (310) 886-9100			Tel: (908) 245-2800

Fax: (310) 886-9119			Fax: (908) 245-2583