SECTION 09802

DECORATIVE FLAKE POLYMERIC FLOOR COATING

Dex-O-Tex Colorflake L

# PART 1.00 – GENERAL

  - GENERAL REQUIREMENTS

- Work of this Section as shown or specified shall be in accordance with the requirements of the Contract Documents

  - WORK INCLUDED

- Work of this section includes all labor materials equipment and services necessary to complete

the decorative flake polymeric floor coating as selected on drawings and/or specified herein.

  - RELATED WORK

- Concrete – Section 03300 (Note to specifier: Concrete should be either water cured or cured using sodium silicate curing compounds only.  Other types of curing compounds are generally not acceptable. Concrete should be cured for a minimum of 28 days. On grade floors should have functioning vapor retarder beneath slab.)

  - SUBMITTALS

- General: Submit the following in accordance with conditions of Contract and Division 1 Specification Sections.

- Product Data: Submit manufacturer’s technical data application instructions and general recommendations for

decorative polymer floor coating specified herein.

C.	LEED Submittals:

1.  	Product Data for Credit MR 4.1 and Credit MR 4.2:  For products having recycled content, submit documentation indicating percentages by weight of postconsumer and preconsumer recycled content.

a.   	Include statement indicating costs for each product having recycled content.

b.	Include LEED Product Information Form for LEED Credits MR 4.1 and 4.2.

2.	Product Data for Credit EQ 4.2:  For field applied, interior, paints coatings and primers, include printed statement of VOC content indicating compliance with Credit requirements.

a.	Include LEED Product Information Form for LEED Credit EQ 4.2.

3.	Provide additional documentation for products as required to achieve each Credit(s).

- Samples for initial selection purposes in form of manufacturer’s color charts showing full range of colors available including white and off-white colors.

- Material certificates signed by manufacturer certifying that the decorative flake polymeric floor coating complies with all regulatory and any requirements specified herein.

- Maintenance Instructions: Submit manufacturer’s written instructions for recommended maintenance practices.

  - QUALITY ASSURANCE

- Installer Qualifications: Engage an experienced Installer or Applicator who specializes in installing resinous floor coating types similar to that required for this Project and who is acceptable to manufacturer of primary materials.

- Single – Source Responsibility: Obtain urethane floor coating materials including primers, resins, hardening agents and finish coats from a single manufacturer.

  - DELIVERY STORAGE AND HANDLING

- Deliver materials in original packages and containers with seals unbroken and bearing manufacturer’s labels containing brand name, directions for storage and mixing with other components.

- Store materials to comply with manufacturer’s directions to prevent deterioration from moisture.

C.	Lighting: Permanent lighting will be in place and working before installing polymeric floor coating.

# PART 2:00 – PRODUCTS

  - MATERIALS

- Decorative flake polymeric floor coating shall be Dex-O-Tex Colorflake L as manufactured by Crossfield Products Corp. in Rancho Dominguez, California and Roselle Park, New Jersey.

  - PROPERTIES

- Colors: As indicated, or if not otherwise indicated, as selected by Architect from manufacturer’s standard colors, which must include white and off-white.

- Physical Properties: Provide floor coatings system that meets or exceeds the listed minimum physical property requirements when tested according to the referenced standard test method in parentheses.

Thickness				15 – 21 mils

Pencil Hardness (ASTM D3363)		3H

Impact Resistance (ASTM D2794)		Direct 50 in. lbs.

Reverse 10 in lbs.

Thermal Shock (ASTM D1211)		Complies

Flexibility (ASTM D1737)		180° Bend (½” Mandrel) Passes

Chemical Resistance (ASTM D1308)

Gasoline				No Effect

Kerosene 			No Effect

Skydrol				No Effect

Isopropyl Alcohol		No Effect

Toluene				No Effect

Hydrogen Peroxide		Slight Stain

Hydrochloric Acid (25%)		No Effect

## PART 3.00 – EXECUTION

  - INSPECTION

- Examine the areas and conditions where the decorative polymeric floor coating is to be installed and notify the Architect of conditions detrimental to the proper and timely completion of the work. Do not proceed with the work until unsatisfactory conditions have been corrected by the Contractor in a manner acceptable to the Architect.

  - PREPARATION

- Substrate: Perform preparation and cleaning procedures according to flooring manufacturer’s instructions for particular substrate conditions involved and as specified. Provide clean, dry and neutral substrate for flooring application.

- Concrete Surfaces: Shot-blast, acid etch or power scarify as required to obtain optimum bond of flooring to concrete. Remove sufficient material to provide a sound surface free laitance, glaze, efflorescence and any bond-inhibiting curing compounds or form release agents. Remove grease, oil and other penetrating contaminates. Repair damaged and deteriorated concrete to acceptable condition. Leave surface free of dust, dirt, laitance and efflorescence.

- Materials: Mix epoxy and polymeric coating components when required and prepare materials according to flooring system manufacturer’s instructions.

  - APPLICATION

- General: Apply each component of decorative flake polymeric floor coating system according to manufacturer’s directions to produce a uniform monolithic flooring surface.

- Bond Coat: Apply epoxy bond coat over prepared substrate at manufacturer’s recommended spreading rate.

- Floor Coating: Over bond coat apply nominal 8-12 DFT thickness Colorflake L Color Coating by roller in two coats at manufacturer’s recommended spreading rate.

- Colorflake: Broadcast PVC color chip into the wet resin to the desire density and color combination as selected and approved.

- Finish Coats: apply two coats clear polymeric enamel over the cured color and PVC broadcast. Lightly sand between coats.

  - CURING, PROTECTION AND CLEANING

- Cure polymeric floor coating materials according to manufacturer’s directions, taking care to prevent contamination during application stages and before completing curing process. Close application area for a minimum of 24 hours.

### END OF SECTION

DEX-O-TEX PRODUCT LINE			3000 E. Harcourt Street		140 Valley Road

Crossfield Products Corp.			Rancho Dominguez, CA 90221		Roselle Park, NJ 07204

www.dexotex.com	.			Tel: (310) 886-9100			Tel: (908) 245-2800

Fax: (310) 886-9119			Fax: (908) 245-2583