# SECTION 09725

# DECORATIVE COLORED FLAKE FLOORING WITH WATERPROOF MEMBRANE

# Dex-O-Tex Colorflake with SC Membrane

# PART 1.00 - GENERAL

# 1.01	GENERAL REQUIREMENTS

A. 	 Work of this Section as shown or specified shall be in accordance with the requirements of the Contract Documents.

# 1.02	 WORK INCLUDED

A.	Work of this Section includes all labor, materials, equipment and services necessary to complete waterproof membrane, epoxy flooring incorporating ceramic coated colored inorganic quartz aggregate and integral base as selected on drawings and/or specified herein.

# 1.03	RELATED WORK

A.	Concrete - Section 03300

(Note to specifier:  Concrete should be either water cured or cured using sodium silicate curing compounds only. Other types of curing compounds are generally not acceptable. Concrete should be cured for a minimum of 28 days.  On grade floors should have functioning vapor retarder beneath slab.)

B.	Floor drains - Division 15

(Note to Specifier:  Floor drains, clean-outs etc. should be of the floor-flange type as manufactured for use with composition floors by most major drain manufacturers.)

# 1.04	SUBMITTALS

A.	General:  Submit the following in accordance with Conditions of Contract and Division 1 Specification Sections.

B.	Product Data:  Submit manufacturer's technical data application instructions and general recommendations for decorative colored flake epoxy flooring specified herein.

C.	LEED Submittals:

1.  	Product Data for Credit MR 4.1 and Credit MR 4.2:  For products having recycled content, submit documentation indicating percentages by weight of postconsumer and preconsumer recycled content.

a.   	Include statement indicating costs for each product having recycled content.

b.	Include LEED Product Information Form for LEED Credits MR 4.1 and 4.2.

2.	Product Data for Credit EQ 4.2:  For field applied, interior, paints coatings and primers, include printed statement of VOC content indicating compliance with Credit requirements.

a.	Include LEED Product Information Form for LEED Credit EQ 4.2.

3.	Provide additional documentation for products as required to achieve each Credit(s).

D.	Samples for initial selection purposes in form of manufacturer's color charts showing range of standard colors available.

1.  Submit 2-1/2" x 4" samples in color and colored flake combination as selected.

E.	Material certificates signed by manufacturer certifying that the decorative colored flake flooring submitted complies with requirements specified herein.

F.	Maintenance Instructions:  Submit manufacturer's written instructions for recommended maintenance practices.

# 1.05   	QUALITY ASSURANCE

A.	Installer Qualifications:  Engage an experienced installer or applicator who has specialized in installing resinous flooring types similar to that required for this Project and who is acceptable to manufacturer of primary materials.

B.	Single-Source Responsibility:  Obtain epoxy component of flooring materials, including primers, resins, hardening agents, and finish or sealing coats, from a single manufacturer.  Obtain colored flake aggregate from primary manufacturer of that product.

# 1.06	DELIVERY STORAGE AND HANDLING

A.	Deliver materials in original packages and containers with seals unbroken and bearing manufacturer's labels containing brand name and directions for storage and    mixing with other components.

B. 	Store materials to comply with manufacturer's directions to prevent deterioration from moisture, heat, cold, direct sunlight, or other detrimental effects.

# 1.07	PROJECT CONDITIONS

A.	Environmental Conditions:  Comply with epoxy resin composition flooring manufacturer's directions for maintenance of ambient and substrate temperature, moisture, humidity, ventilation, and other conditions required to execute and protect work.

B.	Lighting:  Permanent lighting will be in place and working before installing decorative quartz epoxy flooring.

# PART 2:00 - PRODUCTS

# 2.01	MATERIALS

A.	Decorative colored flake flooring and waterproof  membrane shall be Dex-O-Tex Colorflake and Cheminert SC Membrane as manufactured by Crossfield Products Corp. in Rancho Dominguez, California and Roselle Park, New Jersey.

# 2.02	PROPERTIES

A.	Colors: As indicated, or if not otherwise indicated, as selected by Architect from manufacturer's standard color combinations.

B.	Physical Properties:  Provide flooring system that meets or exceeds the listed minimum physical property requirements when tested according to the referenced standard test method in parentheses.

Membrane

Tensile Strength	77ºF

Tensile	1,500 psi

Tensile Elongation	17,150 psi

Tear Strength	120

COLORFLAKE FLOORING

Compressive Strength ASTM D695……………….……………… 9,000 psi

Tensile Strength ASTM D638	….…………………1,200 psi

Hardness ASTM D2240 Shore D	………………… 80-85

Impact Resistance ASTM D2794 	…………………… Passes

Flexibility ASTM D1737**,

180o Bend, 3/4” Mandrel………………………………………...Passes

Adhesion ASTM D4541	…………………….>400 psi

(100% failure in concrete)

Thermal Shock Resistance ASTM D1211*

Cycle of immersion in boiling water 10 mins.

Followed by ice water 10 min. …………………………….Passes 6 cycles

Co-efficient of Static Friction ASTM F609

Dry – Rubber 0.68,	Leather 0.71

Microbial Resistance ASTM G21	………………………….Passes Rating 1

Chemical Resistance

(See Chemical Resistance Chart for Additional Data)

(ASTM D1308/Spot Test Uncovered for 24 hours)

| Betadine | Slight Stain |
| --- | --- |
| Gasoline | No effect |
| Hydraulic Fluid | No effect |
| Hydrochloric Acid 30% | No effect |
| Hydrogen Peroxide 50% | No effect |
| Isopropyl Alcohol | No effect |
| Motor Oil | No effect |
| Nitric Acid 20% | No effect |
| Phosphoric Acid 20% | No effect |
| Salt Water | No effect |
| Skydrol | No effect |
| Sodium Hypochlorite 15% | No effect |
| Sodium Hydroxide 50% | No Effect |
| Sulfuric Acid 50% | No effect |
| Toluene (Toluol) | No effect |

# 2.03	SUPPLEMENTAL MATERIALS

A.	Anti-Microbial Additive:  Incorporate antimicrobial chemical additive to control growth of most bacteria, fungi, algae and actinomycetes. (Note to Specifier:  The use of antimicrobial additive is optional. Its use poses no health hazard.)

B.	Vapor Control Primer Membrane:  Type recommended or produced by manufacturer of epoxy mosaic composition flooring system for type of service and floor condition indicated.

(Note to Specifier:  The use of a Vapor Control Primer membrane is optional and is generally confined to Substrates with An MVER of 3lbs/24hrs/1000SF,  85% rh, or more than 6% residual moisture content All areas requiring membrane treatment should be clearly shown on plans and finish schedules.)

# PART 3.00 - EXECUTION

# 3.01	INSPECTION

A.	Examine the areas and conditions where decorative colored flake flooring is to be installed and notify the Architect of conditions detrimental to the proper and timely completion of the work.  Do not proceed with the work until unsatisfactory conditions have been corrected by the Contractor in a manner acceptable to the Architect.

B.	Moisture Testing: Perform testing for excessive moisture in building components. Test in accordance with ASTM F 1907, provide a written report indicating the test results and if the results are acceptable to proceed with the work. Do not proceed with the work until unsatisfactory conditions have been corrected by the Contractor in a manner acceptable to the Architect.

# 3.02	PREPARATION

A.	Substrate:  Perform preparation and cleaning procedures according to flooring manufacturer's instructions for particular substrate conditions involved, and as specified.  Provide clean, dry, and neutral substrate for flooring application.

B.	Concrete Surfaces:  Shot-blast, acid etch or power scarify as required to obtain optimum bond of flooring to concrete. Remove sufficient material to provide a sound surface, free of laitance, glaze, efflorescence, and any bond-inhibiting curing compounds or form release agents.  Remove grease, oil, and other penetrating contaminates. Repair damaged and deteriorated concrete to acceptable condition. Leave surface free of dust, dirt, laitance, and efflorescence.

C.	Materials:  Mix epoxy resin components when required, and prepare materials according to flooring system manufacturer's instructions.

# 3.03	APPLICATION

A.	General:  Apply each component of epoxy mosaic composition flooring system according to manufacturer's directions to produce a uniform monolithic flooring surface of thickness indicated.

Bond Coat:  Apply bond coat over prepared substrate at manufacturer's recommended spreading rate.

Detailing: Detail all Cracks, Joints, Terminations and Transitions. Perform all recommended preparation and detailing with Cheminert SC Membrane and reinforcing fabric. Apply detail coat at all horizontal vertical junctures. Turn Cheminert SC Membrane up the vertical surfaces a minimum 3”. Allow to cure.

Membrane: Apply flexibilized chemical resistant epoxy membrane to a dry film thickness of 40 mils, allow to cure.  Apply to base at height of 3” or as shown on plans.

Floor Coating: Over bond coat apply nominal 8-12 DFT thickness Colorflake L Color Coating by roller in two coats at manufacturer’s recommended spreading rate.

Colorflake: Broadcast PVC color chip into the wet resin to the desire density and color combination as selected and approved.

Finish or Sealing Coats: After quartz filled broadcast coats have cured sufficiently, apply finish coats of type recommended by flooring manufacturer to produce finish matching approved submittal sample and in number of coats and spreading rates recommended by manufacturer. Finished floor shall be 1/16"-1/8" thick, uniform in color and free of trowel marks

Cove Base: Apply cove base mix to wall surfaces at locations shown to form cove base height of 4 inches unless otherwise indicated. Follow manufacturer's printed instructions and details including taping, mixing, priming, troweling, sanding, and top-coating of cove base.

# 3.04	CURING, PROTECTION AND CLEANING.

A.	Cure decorative quartz epoxy flooring materials according to manufacturer's directions, taking care to prevent contamination during application stages and before completing curing process.  Close application area for a minimum of 24 hours.

# END OF SECTION

DEX-O-TEX PRODUCT LINE		3000 E. Harcourt Street		     140 Valley Road

Crossfield Products Corp.			Rancho Dominguez, CA 90221	     Roselle Park, NJ 07204

www.dexotex.com			Tel: (310) 886-9100		     Tel: (908) 245-2800

Fax: (310) 886-9119		     Fax: (908) 245-2583