# SECTION 09725

# DECORATIVE QUARTZ EPOXY FLOORING

# Dex-O-Tex Decor-Flor

# PART 1.00 - GENERAL

# 1.01	GENERAL REQUIREMENTS

A. 	 Work of this Section as shown or specified shall be in accordance with the requirements of the Contract Documents.

# 1.02	 WORK INCLUDED

A.	Work of this Section includes all labor, materials, equipment and services necessary to complete epoxy flooring incorporating ceramic coated colored inorganic quartz aggregate and integral base as selected on drawings and/or specified herein.

# 1.03	RELATED WORK

A.	Concrete - Section 03300

(Note to specifier:  Concrete should be either water cured or cured using sodium silicate curing compounds only. Other types of curing compounds are generally not acceptable. Concrete should be cured for a minimum of 28 days.  On grade floors should have functioning vapor retarder beneath slab.)

B.	Floor drains - Division 15

(Note to Specifier:  Floor drains, clean-outs etc. should be of the floor-flange type as manufactured for use with composition floors by most major drain manufacturers.)

# 1.04	SUBMITTALS

A.	General:  Submit the following in accordance with Conditions of Contract and Division 1 Specification Sections.

B.	Product Data:  Submit manufacturer's technical data application instructions and general recommendations for decorative quartz epoxy flooring specified herein.

C.	LEED Submittals:

1.  	Product Data for Credit MR 4.1 and Credit MR 4.2:  For products having recycled content, submit documentation indicating percentages by weight of postconsumer and preconsumer recycled content.

a.   	Include statement indicating costs for each product having recycled content.

b.	Include LEED Product Information Form for LEED Credits MR 4.1 and 4.2.

2.	Product Data for Credit EQ 4.2:  For field applied, interior, paints coatings and primers, include printed statement of VOC content indicating compliance with Credit requirements.

a.	Include LEED Product Information Form for LEED Credit EQ 4.2.

3.	Provide additional documentation for products as required to achieve each Credit(s).

D.	Samples for initial selection purposes in form of manufacturer's color charts showing range of standard colors available.

1.  Submit 2-1/2" x 4" samples in color and quartz aggregate combination as selected.

E.	Material certificates signed by manufacturer certifying that the decorative quartz epoxy flooring submitted complies with requirements specified herein.

F.	Maintenance Instructions:  Submit manufacturer's written instructions for recommended maintenance practices.

# 1.05   	QUALITY ASSURANCE

A.	Installer Qualifications:  Engage an experienced installer or applicator who has specialized in installing resinous flooring types similar to that required for this Project and who is acceptable to manufacturer of primary materials.

B.	Single-Source Responsibility:  Obtain epoxy component of flooring materials, including primers, resins, hardening agents, and finish or sealing coats, from a single manufacturer.  Obtain ceramic-coated quartz aggregate from primary manufacturer of that product.

# 1.06	DELIVERY STORAGE AND HANDLING

A.	Deliver materials in original packages and containers with seals unbroken and bearing manufacturer's labels containing brand name and directions for storage and    mixing with other components.

B. 	Store materials to comply with manufacturer's directions to prevent deterioration from moisture, heat, cold, direct sunlight, or other detrimental effects.

# 1.07	PROJECT CONDITIONS

A.	Environmental Conditions:  Comply with epoxy resin composition flooring manufacturer's directions for maintenance of ambient and substrate temperature, moisture, humidity, ventilation, and other conditions required to execute and protect work.

B.	Lighting:  Permanent lighting will be in place and working before installing decorative quartz epoxy flooring.

# PART 2:00 - PRODUCTS

# 2.01	MATERIALS

A.	Decorative quartz epoxy flooring shall be Dex-O-Tex Decor-Flor as manufactured by Crossfield Products Corp. in Rancho Dominguez, California and Roselle Park, New   Jersey.

# 2.02	PROPERTIES

A.	Colors: As indicated, or if not otherwise indicated, as selected by Architect from manufacturer's standard color combinations.

B.	Physical Properties:  Provide flooring system that meets or exceeds the listed minimum physical property requirements when tested according to the referenced standard test method in parentheses.

# Compressive Strength

Complete System (ASTM C109)			8,556 psi.

Resin Component (ASTM D695)			12,900 psi.

Surface Hardness (ASTM D2240)		             	Durometer D 85

Aggregate Hardness (Moh's Mineral Scale)              	 6 1/2-7

Indentation Characteristics (MIL-PRF-3134)

Para. 4.7.4.2.1-Steadily Applied Load)		0.005 indentation

Impact Resistance (MIL-PRF-3134)		0.011 indentation

Para. (4.7.3)						No cracking, loss of bond

Adhesion (ACI Comm. 503.1-92)			345 psi. (100% failure in concrete)

Water Absorption (MIL-PRF-3134)		Less than 1%

Abrasion Resistance (ASTM C501)			19 Wear Index (H-22 Wheel)

Tensile Strength (ASTM D638)          		4,400 psi.

Resin Component

Elongation (ASTM D638)				19.6%

Resin Component

# 2.03	SUPPLEMENTAL MATERIALS

A.	Waterproofing Membrane:  Type recommended or produced by manufacturer of epoxy resin composition flooring system for type of service and floor condition indicated. (Note to Specifier:  The use of waterproof membrane is optional and is generally confined to suspended floors and in rooms having floor drains and subject to very wet spillage and service.  All areas requiring membrane treatment should be clearly shown on plans and finish schedules.)

B.	Anti-Microbial Additive:  Incorporate antimicrobial chemical additive to control growth of most bacteria, fungi, algae and actinomycetes. (Note to Specifier:  The use of antimicrobial additive is optional. Its use poses no health hazard.)

# PART 3.00 - EXECUTION

# 3.01	INSPECTION

A.	Examine the areas and conditions where decorative quartz epoxy flooring is to be installed and notify the Architect of conditions detrimental to the proper and timely completion of the work.  Do not proceed with the work until unsatisfactory conditions have been corrected by the Contractor in a manner acceptable to the Architect.

# 3.02	PREPARATION

A.	Substrate:  Perform preparation and cleaning procedures according to flooring manufacturer's instructions for particular substrate conditions involved, and as specified.  Provide clean, dry, and neutral substrate for flooring application.

B.	Concrete Surfaces:  Shot-blast, acid etch or power scarify as required to obtain optimum bond of flooring to concrete. Remove sufficient material to provide a sound surface, free of laitance, glaze, efflorescence, and any bond-inhibiting curing compounds or form release agents.  Remove grease, oil, and other penetrating contaminates. Repair damaged and deteriorated concrete to acceptable condition. Leave surface free of dust, dirt, laitance, and efflorescence.

C.	Materials:  Mix epoxy resin components when required, and prepare materials according to flooring system manufacturer's instructions.

# 3.03	APPLICATION

A.	General:  Apply each component of decorative quartz epoxy flooring system according to manufacturer's directions to produce a uniform monolithic flooring surface of thickness indicated.

B.	Broadcast Coats: Apply liberal application of clear epoxy resin mixture, allow to self-level, broadcast (by hand or spray machine) ceramic coated quartz aggregate, allow to set to hardness, sweep off excess unbonded aggregate and repeat process to achieve total        nominal thickness of 1/16"-1/8".

C.	Finish or Sealing Coats: After quartz filled broadcast coats have cured sufficiently, apply finish coats of type recommended by flooring manufacturer to produce finish matching approved submittal sample and in number of coats and spreading rates recommended by manufacturer.

1.  Finished floor shall be 1/16"-1/8" thick, uniform in color and free of trowel marks.

D.	Cove Base: Apply cove base mix to wall surfaces at locations shown to form cove base height of 4 inches unless otherwise indicated. Follow manufacturer's printed instructions and details including taping, mixing, priming, troweling, sanding, and top-coating of cove base.

# 3.04	CURING, PROTECTION AND CLEANING.

A.	Cure decorative quartz epoxy flooring materials according to manufacturer's directions, taking care to prevent contamination during application stages and before completing curing process.  Close application area for a minimum of 24 hours.

# END OF SECTION

DEX-O-TEX PRODUCT LINE		3000 E. Harcourt Street		     140 Valley Road

Crossfield Products Corp.			Rancho Dominguez, CA 90221	     Roselle Park, NJ 07204

www.dexotex.com			Tel: (310) 886-9100		     Tel: (908) 245-2800

Fax: (310) 886-9119		     Fax: (908) 245-2583