# PART 1.00 - GENERAL

  - GENERAL REQUIREMENTS

- Work of this Section as shown or specified shall be in accordance with the requirements of the Contract Documents.

  - WORK INCLUDED

A.	Work of this Section includes all labor, materials, equipment and services necessary to complete epoxy flooring incorporating color coated quartz aggregate and integral cove base as selected on drawings and/or specified herein.

  - RELATED WORK

A.	Concrete - Section 03300 – Concrete and concrete placement shall be in compliance with ACI 302, ACI 224, ACI 503 and other applicable standards.

(Note to Specifier:  Concrete should be either water cured or cured using sodium silicate curing compounds only. Other types of curing compounds are generally not acceptable. Concrete should be cured for a minimum of 28 days, while concrete containing fly ash should be cured for a minimum of 56 days.  On grade floors must have functioning vapor retarder barrier in compliance with ACI 302 beneath slab.)

B.	 Floor drains - Division 15 – Concrete must be adequately sloped to drain prior to placement of the Decor-Flor Troweled system.

(Note to Specifier:  Floor drains, clean-outs etc. should be of the floor-flange type as manufactured for use with composition floors by most major drain manufacturers.)

  - SUBMITTALS

- General:  Submit the following in accordance with Conditions of Contract and Division 1 Specification Sections.

- Product Data:  Submit manufacturer's technical data application instructions and general recommendations for decorative colored quartz troweled epoxy flooring specified herein.

C.	LEED Submittals:

1.  	Product Data for Credit MR 4.1 and Credit MR 4.2:  For products having recycled content, submit documentation indicating percentages by weight of postconsumer and preconsumer recycled content.

a.   	Include statement indicating costs for each product having recycled content.

b.	Include LEED Product Information Form for LEED Credits MR 4.1 and 4.2.

2.	Product Data for Credit EQ 4.2:  For field applied, interior, paints coatings and primers, include printed statement of VOC content indicating compliance with Credit requirements.

a.	Include LEED Product Information Form for LEED Credit EQ 4.2.

3.	Provide additional documentation for products as required to achieve each Credit(s).

D.	Samples for initial selection purposes in form of manufacturer's color charts showing range of standard colors available.

E.	Submit 2-1/2" x 4" samples in colored quartz aggregate combination as selected.

F.	Material certificates signed by manufacturer certifying that the decorative colored quartz troweled epoxy flooring submitted complies with requirements specified herein.

G.	Maintenance Instructions:  Submit manufacturer's written instructions for recommended maintenance practices.

  - QUALITY ASSURANCE

A.	Installer Qualifications:  Engage an experienced installer or applicator who has specialized in installing resinous flooring types similar to that required for this Project and who is acceptable to manufacturer of primary materials.

B.	Single-Source Responsibility:  Obtain epoxy component of flooring materials, including primers, resins, hardening agents, and finish or sealing coats, from a single manufacturer. Obtain color coated quartz aggregate from primary manufacturer of that product.

  - DELIVERY STORAGE AND HANDLING

A.	Deliver materials in original packages and containers with seals unbroken and bearing manufacturer's labels containing brand name and directions for storage and    mixing with other components.

B. 	Store materials to comply with manufacturer's directions to prevent deterioration from moisture, heat, cold, direct sunlight, or other detrimental effects.

  - PROJECT CONDITIONS

A.	Environmental Conditions:  Comply with epoxy resin composition flooring manufacturer's directions for maintenance of ambient and substrate temperature, moisture, humidity, ventilation, and other conditions required to execute and protect work.

B.	Lighting:  Permanent lighting will be in place and working before installing decorative quartz epoxy flooring.

# PART 2:00 - PRODUCTS

  - MATERIALS

A.	Decorative colored quartz troweled epoxy flooring shall be Dex-O-Tex Decor-Flor as manufactured by Crossfield Products Corp., in Rancho Dominguez, California and Roselle Park, New Jersey

  - PROPERTIES

A.	Colors: As indicated, or if not otherwise indicated, as selected by Architect from manufacturer's standard color combinations.

B.	Physical Properties:  Provide flooring system that meets or exceeds the listed minimum physical property requirements when tested according to the referenced standard test method in parentheses.

# TYPICAL PHYSICAL PROPERTIES at 75oF (24oC)

Compressive Strength ASTM C579	10,500 psi

(Resin, Hardener & Aggregate) 	(738 kg/cm2)

Compressive Strength ASTM D695	12,900 psi

(Resin & Hardener)	(907 kg/cm2)

Tensile Strength ASTM C307	 1,800 psi

(Resin, Hardener & Aggregate) 	 (127 kg/cm2)

Tensile Strength ASTM D638	5,000 psi

(Resin & Hardener)	(352 kg/cm2)

Flexural Strength ASTM C580	4,000 psi

(281 kg/cm2)

Surface Hardness ASTM D2240 Shore D	  80-85

Indentation Characteristics

(Steadily Applied Load) MIL-PRF-3134,	0.005”

Para. 4.7.4.2.1, 2000 lbs on                                                   (0.127 mm)

1” steel ram imposed for 30 minutes over

a concrete substrate, indented

Indentation Characteristics MIL-PRF-3134, Para. 4.7.3

(Impact Load) 	0.011”

(2 lb . . . 908 kg.) Indent from steel ball	                (0.28 mm)

dropped twice from 8 ft. height

Adhesion ASTM D4541	> 400 psi

(100% failure in concrete)                                                       (28.1 kg/cm2)

Water Absorption MIL-PRF-3134	< 1.0%

Abrasion Resistance ASTM D4060

(CS17, 1000gr load, 1000 cycles)	0.04 gr

Antimicrobial Resistance ASTM G21	Passes

Flammability ASTM D635	Self-Extinguishing

Bonded to Concrete

  - SUPPLEMENTAL MATERIALS

- Waterproofing or Fluid Proofing Membrane:  Type recommended or produced by manufacturer of epoxy resin composition flooring system for type of service and floor condition indicated.

(Note to Specifier:  The use of waterproofing or fluid proofing membrane is optional and is generally confined to suspended floors and in rooms having floor drains and subject to very wet spillage and service.  All areas requiring membrane treatment should be clearly shown on plans and finish schedules.)

- Anti-Microbial Additive:  Incorporate antimicrobial chemical additive to control growth of most algae, bacteria, fungi, mildew and mold.

(Note to Specifier:  The use of antimicrobial additive is optional. Its use poses no health hazard.)

- Moisture Mitigation System:  Concrete, especially slab on grade should be tested in accordance with ASTM F1869. If pounds exceed flooring limit remedial action must be taken.

(Note to Specifier:  The use of moisture mitigation system may be required if values exceed manufactures published data.)

# PART 3.00 - EXECUTION

  - INSPECTION

A.	Examine the areas and conditions where decorative quartz epoxy flooring is to be installed and notify the Architect of conditions detrimental to the proper and timely completion of the work.  Do not proceed with the work until unsatisfactory conditions have been corrected by the Contractor in a manner acceptable to the Architect.

  - PREPARATION

A.	Substrate:  Perform preparation and cleaning procedures according to flooring manufacturer's instructions for particular substrate conditions involved, and as specified.  Provide clean, dry, and neutral substrate for flooring application.

B.	Concrete Surfaces:  Shot-blast, grind or power scarify as required to obtain optimum bond of flooring to concrete. Profile should match published International Concrete Repair Institute (ICRI) Guideline No. 03731 Guide for Selecting and Specifying Concrete Surface Preparation for Sealers, Coatings and Polymer Overlays. Remove sufficient material to provide a sound surface, free of laitance, glaze, efflorescence, and any bond-inhibiting curing compounds or form release agents.  Remove grease, oil, and other penetrating contaminants. Repair damaged and deteriorated concrete to acceptable condition. Leave surface free of dust, dirt, laitance, and efflorescence.

C.	Materials:  Mix epoxy resin/hardener components when required, and prepare materials according to flooring system manufacturer's instructions.

  - APPLICATION

A.	General:  Apply each component of decorative colored quartz troweled epoxy flooring system according to manufacturer's directions to produce a uniform monolithic flooring surface of thickness indicated.

B.	Troweled Colored Quartz Troweled Flooring System: Mix resin, hardener and blended colored quartz aggregate per the manufacturer’s instruction and place a sufficient amount of material to obtain the specified thickness.

- Groutcoat: Grout the Troweled Colored Quartz Epoxy Flooring System to fill the indices (voids) in the system, which may require one or more groutcoats depending on surface porosity.

- Finish or Sealing Coats: After groutcoat(s) has cured sufficiently, apply finishcoats of type recommended by flooring manufacturer to produce finish matching approved submittal sample and in number of coats and spreading rates recommended by manufacturer.

- Finished floor shall be 3/16"-1/4" thick, uniform in color and free of excessive trowel marks.

- Cove Base: Apply cove base mix to wall surfaces at locations specified at a height of 4 inches unless otherwise indicated. Follow manufacturer's printed instructions and details including taping, mixing, priming, troweling, sanding, and top-coating of cove base.

  - CURING, PROTECTION AND CLEANING.

A.	Cure decorative quartz epoxy flooring materials according to manufacturer's directions, taking care to prevent contamination during application stages and before completing curing process.  Close application area for a minimum of 24 hours.

# END OF SECTION

DEX-O-TEX PRODUCT LINE		3000 E. Harcourt Street		140 Valley Road

Crossfield Products Corp.			Rancho Dominguez, CA 90221	Roselle Park, NJ 07204

www.dexotex.com			Tel: (310) 886-9100		Tel: (908) 245-2800

Fax: (310) 886-9119		Fax: (908) 245-2583