SECTION 07570

TRAFFIC-BEARING ROOF DECK SURFACING

Dex-O-Tex Weatherwear Microtopping Finish

PART 1.00 - GENERAL

1.01	GENERAL REQUIREMENTS

A.	Work of this Section, as shown or specified, shall be in accordance with the requirements of the Contract Documents.

1.02	WORK INCLUDED

- Work of this Section includes all labor, materials, equipment and services necessary to complete the waterproof neoprene composition traffic bearing roof deck surfacing as scheduled on the drawings and/or specified herein.

1.03	RELATED WORK

A.	Concrete - Section 03300.

(Note to Specifier:  Concrete slab should be either water cured or cured using sodium silicate curing compounds only.  Other types of curing compounds are generally not acceptable.  Concrete should be cured for a minimum of 28 days with maximum moisture content of 7%. Lightweight concrete topping slabs should not contain lightweight aggregates such as gypsum or vermiculite. Structural concrete and concrete topping shall include expansion joints and expansion joints shall be filled with Dex-O-Tex Elastatex 500 joint filling compound or approved equal.  Minimum pitch of 1/8 inch per foot. On grade floors should have vapor retarder beneath slab and be properly vented.)

B.	Floor drains - Division 15.

(Note to Specifier:  Floor drains, clean-outs, etc. should be of the "floor-flange" type as manufactured for use with composition floors by most major drain manufacturers. Drain flange shall be finished flush with substrate.)

C.	Insulation, vapor barrier and protective waterproofing

(Consult Crossfield Products Corp. for specific recommendation)

D.	Sheet metal flashing

(Note to Specifier: Sheet metal flashing shall be minimum 26-gauge bonderized. All joint or seams shall be caulked with Dex-O-Tex Elastatex 500 flashing paste or approved equal.)

E.	Plywood substrate including framing and blocking

(Note to Specifier: Plywood shall be a minimum 5/8 inch (preferably 3/4 inch) exterior grade.  Plywood shall have 2.5 expanded metal lath attached mechanically attached and filled with Dex-O-Tex A-81 or G-26 underlayment. Plywood shall be supported 16" on center and properly blocked. Plywood shall be attached with either screws or screw type or ring shank nails.)

F.	Slope for drainage

(Note to Specifier: allow minimum 1/8 inch per foot slope to drain. This can be provided for in the substrate or by application of Dex-O-Tex G-26 underlayment. Care must be taken to provide adequate elevation at thresholds to provide proper slope to drain.)

G.	Wall vents

(Note to Specifier: Wall vents are used to relieve moisture vapor transmission pressure from beneath the waterproof membrane of the waterproof deck covering system. Moisture vapor commonly collect in areas below a vapor barrier such as the waterproof membrane of the deck covering system. These vents should be installed in the flashing on any deck larger then 500 square feet, or approximately one vent every 300 square feet)

1.04    SUBMITTALS

A.	General:  Submit the following in accordance with Conditions of Contract and Division 1 Specification Sections.

B.	Product Data: Submit manufacturer's technical data, application instructions and general recommendations for the waterproof neoprene composition traffic bearing roof deck surfacing specified herein.

C.	LEED Submittals:

1.  	Product Data for Credit MR 4.1 and Credit MR 4.2:  For products having recycled content, submit documentation indicating percentages by weight of postconsumer and preconsumer recycled content.

a.   	Include statement indicating costs for each product having recycled content.

b.	Include LEED Product Information Form for LEED Credits MR 4.1 and 4.2.

2.	Product Data for Credit EQ 4.2:  For field applied, interior, paints coatings and primers, include printed statement of VOC content indicating compliance with Credit requirements.

a.	Include LEED Product Information Form for LEED Credit EQ 4.2.

3.	Provide additional documentation for products as required to achieve each Credit(s).

D.	Samples for initial selection purposes in form of manufacturer's color charts showing full range of colors and finishes available.

1. Submit 2- 12” X 12”" samples of color chips from color chart selection designated by the Architect.

E.	Material certificates signed by manufacturer certifying that the waterproof neoprene composition traffic bearing roof deck surfacing complies with requirements specified herein.

F.	Maintenance Instructions:  Submit manufacturer's written instructions for recommended maintenance practices.

G.	Provide a copy of I.C.B.O. test report stating that the proposed neoprene composition traffic bearing roof deck system is class A fire rated, and has met all I.C.B.O. criteria for walking decks.

1.05	QUALITY ASSURANCE

A.	Installer Qualifications: Engage an experienced Installer or applicator who has specialized in installing waterproof deck covering system types similar to that required for this Project and who is acceptable to manufacturer of primary materials.

B.	Single-Source Responsibility:  Obtain waterproof neoprene composition traffic bearing roof deck surfacing materials, including primers, resins, hardening agents, and finish or sealing coats, from a single manufacturer.

C.	Pre-Qualified Suppliers: Submit any request for alternative products for review two weeks prior to bid date.  Any request for alternate products received after this date will not be considered.

1.06	DELIVERY, STORAGE AND HANDLING

A.	Deliver materials in original packages and containers with seals unbroken and bearing manufacturer's labels containing brand name and directions for storage and mixing with other components.

B.	Comply with manufacturer's directions for materials storage to prevent deterioration from moisture, heat, cold, direct sunlight, or other detrimental effects.

1.07	PROJECT CONDITIONS

A.	Environmental Conditions: Comply with waterproof neoprene composition traffic bearing roof deck surfacing manufacturer's directions for maintenance of ambient and substrate temperature, moisture, humidity, ventilation, and other conditions required to execute and protect work.

PART 2.00 PRODUCTS

2.01	MATERIALS

A.	Troweled waterproof neoprene composition traffic bearing roof deck surfacing shall be Dex-O-Tex Weatherwear as manufactured by Crossfield Products Corp. in Rancho Dominguez, California and Roselle Park, New Jersey.

B.	The Trowel applied waterproof neoprene composition traffic bearing roof deck surfacing system shall be composed of a slip-sheet, waterproof membrane, traffic surfacing and finish coats, and shall conform to the following standards:

1.) Traffic deck binder and all rubber emulsions shall be compounded with neoprene liquid and shall have a minimum neoprene solids content of 35% when tested by the dry cup method.

2.) Aggregate for traffic surface coating shall be suitably graded fine trap-rock passing a #20 mesh sieve and retained on a #40 mesh sieve.

3.) Waterproof Membrane shall consist of a neoprene based asphalt extended mastic with a minimum elongation of 1100 % when unreinforced.

4.) Fabric used as reinforcement for waterproofing shall be 7 1/2 oz. woven polypropylene fabric.

5.) Final Finish dressing shall be a single component, water-phase acrylic latex emulsion material, pigmented and of a consistency suitable for roller application.

2.02	PROPERTIES

A.	Colors:  As indicated, or if not otherwise indicated, as selected by Architect from manufacturer's standard colors.

B.	Physical Properties:

Provide a waterproof deck covering system that meet or exceed the listed minimum physical property requirements when tested according to the referenced standard test method in parentheses.

Weight					2.5 lbs. per Sq.Ft.

Accelerated Weatherwear RS II (ASTM G23)	No cracking, blistering, delamination

chalking, crazing or color change

Accelerated Aging (ASTM D756)			No cracking, blistering, delamination

chalking, crazing or color change

Freeze-Thaw (ASTM C67)			No breakage or weight loss

Abrasion (ASTM D1242)			4.3% @ No. 80TP

Percolation (ICBO standard)			Complies

Water Absorption (ASTM D570)			<6.09% No warping or cracking

Wind Uplift (ICBO Factory Mutual 1-52)	Complies 131 MPH @ 3 Safety factor

Flammability (ASTM E108, UL 790, NFPA 256)

Intermittent Flame Exposure		Class A

Spread of Flame				Class A

Burning Brand				Class A

Chemical Resistance

Industrial Detergent			No change in texture or color

Salt (20%)				No change in texture or color

Ammonia Solution (5%)			No change in texture or color

Muriatic Acid (10%)			No change in texture or color

Chlorine (10%)				No change in texture or color

Kerosene				No change in texture or color

Turpentine				Slight temporary softening of surface

Paint thinner				Slight Temporary softening of surface

2.03    SUPPLEMENTAL MATERIALS

A.	Optional Decorative Finishes: Type recommended or produced by manufacturer of waterproof neoprene composition traffic bearing roof deck surfacing system to achieve desired color, texture, pattern and finish

(Note to Specifier:  The use of a decorative finish is optional and is available in numerous finishes. The decorative finish of the decking system will vary depending on installation technique and inherent properties of various fillers and aggregates which may be incorporated in finish system. It is essential to choose the proper finish required for your specific application. Once a pattern, texture, and colors are selected, approved submittal samples will accurately depict the actual final finish of the decorative waterproof deck covering system. All areas to receive an other than standard finish shall be clearly shown on plans and finish schedules.)

- Optional Top Coat: Type recommended or produced by manufacturer of waterproof neoprene composition traffic bearing roof deck system for any specific chemical resistance, skid resistance or profile of desired final finish.

(Note to Specifier: The final finish of the decking system will vary depending on installation technique and inherent properties which may be incorporated in finish system. It is essential to choose the proper finish required for your specific application. Once a final finish is selected, approved submittal samples will accurately depict the actual final finish of the waterproof deck covering system.)

PART 3.00 - EXECUTION

3.01	INSPECTION

A.	Examine the areas and conditions where the waterproof neoprene composition traffic bearing roof deck surfacing is to be installed and notify the Architect of conditions detrimental to the proper and timely completion of the work.  Do not proceed with the work until unsatisfactory conditions have been corrected by the Contractor in a manner acceptable to the Architect.

B.	Evaluate level of moisture in the substrate to determine that moisture levels are acceptable for application of specified waterproof deck covering system.

3.02     PREPARATION

A.	Substrate:  Perform preparation and cleaning procedures according to waterproof deck covering manufacturer's instructions for particular substrate conditions involved, and as specified.  Provide clean, dry and neutral substrate for application of waterproof deck covering.

B.	Materials:  Mix aqueous emulsions and aggregate when required as per manufacturer's instructions. Prepare materials according to waterproof deck covering system manufacturer's instructions.

3.03	APPLICATION

A.	General:  Apply each component of waterproof neoprene composition traffic bearing roof deck surfacing system according to manufacturer's directions to produce a uniform monolithic surface of thickness indicated.

B.	Apply Slip-Sheet of properly prepared substrate. Overlap seams a minimum of 2 inches. Apply latex bonding coat when required.

C.	Apply reinforced membrane at all vertical junctures. Embed polypropylene fabric into neoprene membrane liquid.

D.	Apply aqueous neoprene rubber waterproof membrane solution with glass fabric reinforcement to entire area to be coated. Overlap all seams a minimum of 2 inches.

E.	Trowel apply two coats of neoprene and aggregate composition traffic surfacing over all surfaces previously covered with waterproof membrane.  Sand surface to remove trowel marks or small surface imperfections.

F.	Trowel apply top traffic coats of cementitious co-polymer and fine aggregate composition to achieve desired surface. Sand to remove trowel marks or small surface imperfections and to expose mottled appearance

G.	Roller apply two coats of clear sovenated acrylic final finish dressing to a uniform finish.

H.	Finished neoprene composition traffic-bearing roof deck surfacing shall be a nominal 3/16 inch thick, smooth and uniform in color and texture.

(Note to Specifier: For installation of decorative finishes consult Crossfield Products Corp.)

3.04      CURING, PROTECTION AND CLEANING

A.	Cure waterproof neoprene composition traffic bearing roof deck surfacing materials according to manufacturer's directions, taking care to prevent contamination during application stages and before completing curing process.  Close application area for a minimum of 24 hours.

## END OF SECTION

DEX-O-TEX PRODUCT LINE		3000 E. Harcourt Street			140 Valley Road

Crossfield Products Corp.			Rancho Dominguez, CA 90221		Roselle Park, NJ 07204

www.dexotex.com			Tel: (310) 886-9100			Tel: (908) 245-2800

Fax: (310) 886-9119			Fax: (908) 245-2583