# SECTION 07574

# Fracture Resistant Waterproof Membrane System

# Thin-set Tile over Plywood Substrate

# Dex-O-Tex Neobond

# PART 1.00 - GENERAL

# 1.01	GENERAL REQUIREMENTS

A.	Work of this Section, as shown or specified, shall be in accordance with the requirements of the Contract Documents.

# 1.02	WORK INCLUDED

A.	Work of this Section includes all labor, materials, equipment and services necessary to complete surface preparation, attachment of metal lath, application of a polyacrylate smoothing leveling coat, and application of the waterproof neoprene composition fracture resistant waterproof membrane system and traffic topping as scheduled on the drawings and/or specified herein.

# 1.03	RELATED WORK

A.	Plywood Substrate.

(Plywood Substrate shall be a minimum of 5/8” cdx or other exterior grade. Screwed or nailed with ring shank or screw type nails on the perimeter 8” O.C. and in the field a minimum of 16” O.C.)

B.	Floor drains - Division 15.

(Note to Specifier:  Floor drains, clean-outs, etc. should be of the "floor-flange" type as manufactured for use with composition floors by most major drain manufacturers. Drain flange shall be finished with substrate. Bi-Level drains shall be used with mortar bed installations)

C.	 Flashing

(Note to Specifier:  Sheet metal flashing shall be minimum 26 gauge galvanized. All joint or seams shall be overlapped approx. 3" and caulked with Dex-O-Tex Elastatex 500 flashing paste or approved equal.)

E.	 Slope for drainage

(Note to Specifier: A recommended 1/8 inch per foot slope to drain. This can be provided for in the substrate or by application of Dex-O-Tex A-81 Underlayment prior to application of the Neobond system. Care must be taken to provide adequate elevation at thresholds to provide proper slope to drain.)

1.04    SUBMITTALS

A.	General:  Submit the following in accordance with Conditions of Contract and Division 1 Specification Sections.

B.	Product Data:  Submit manufacturer's technical data, application instructions and general recommendations for the underlayment and waterproof neoprene composition fracture Resistant waterproof membrane system specified herein.

C.	LEED Submittals:

1.  	Product Data for Credit MR 4.1 and Credit MR 4.2:  For products having recycled content, submit documentation indicating percentages by weight of postconsumer and preconsumer recycled content.

a.   	Include statement indicating costs for each product having recycled content.

b.	Include LEED Product Information Form for LEED Credits MR 4.1 and 4.2.

2.	Product Data for Credit EQ 4.2:  For field applied, interior, paints coatings and primers, include printed statement of VOC content indicating compliance with Credit requirements.

a.	Include LEED Product Information Form for LEED Credit EQ 4.2.

3.	Provide additional documentation for products as required to achieve each Credit(s).

D.	Samples for initial selection purposes in form of manufacturer's recommended installation procedures for specific application parameters.

E.	Material certificates signed by manufacturer certifying that the waterproof neoprene composition fracture Resistant waterproof membrane system complies with requirements specified herein.

F.	Maintenance Instructions:  Submit manufacturer's written instructions for recommended maintenance practices.

G.	Provide a copy of Ceramic Tile Institute (C.T.I.) approval stating that the proposed neoprene composition fracture Resistant membrane system is approved and has met all C.T.I. criteria for waterproof membranes.

# 1.05	QUALITY ASSURANCE

A.	Installer Qualifications:  Engage an experienced Installer or applicator who has specialized in installing waterproof deck covering system types similar to that required for this Project and who is acceptable to manufacturer of primary materials.

B.	Single-Source Responsibility:  Obtain waterproof neoprene composition fracture Resistant waterproof membrane system, underlayments and traffic topping materials, including primers, resins, hardening agents, and finish or sealing coats, from a single manufacturer.

C.	Pre-Qualified Materials: Submit any request for alternative products for review two weeks prior to bid date.  Any request for alternate products received after this date will not be considered.

1.06	DELIVERY, STORAGE AND HANDLING

A.	Deliver materials in original packages and containers with seals unbroken and bearing manufacturer's labels containing brand name and directions for storage and mixing with other components.

B.	Comply with manufacturer's directions for materials storage to prevent deterioration from moisture, heat, cold, direct sunlight, or other detrimental effects.

# 1.07	PROJECT CONDITIONS

A.	Environmental Conditions:  Comply with waterproof neoprene composition fracture Resistant waterproof membrane system manufacturer's directions for maintenance of ambient and substrate temperature, moisture, humidity, ventilation, and other conditions required to execute and protect work.

# PART 2.00 PRODUCTS

# 2.01	MATERIALS

A.	Troweled waterproof neoprene composition fracture Resistant waterproof membrane system shall be Dex-O-Tex Neobond below tile waterproof membrane, Underlayment shall be Dex-O-Tex A 81 Underlayment and protection topping shall be Dex-O-Tex Resistite as manufactured by Crossfield Products Corp. in Rancho Dominguez, California and Roselle Park, New Jersey.

B.	The underlayment, trowel applied waterproof neoprene composition fracture Resistant waterproof membrane, and traffic topping system shall be composed of the following:

1.  Smoothing coat of A-81 Underlayment. Any slope for drainage should be accomplished with   this application.

2.  Waterproof membrane.

3.  Protection Topping

And shall conform to the following standards:

a.)	All resin binders and all rubber emulsions shall be compounded with neoprene or polyacyralate Co-Polymer liquids and shall have a minimum polymer or neoprene solids content of 35% when tested by the dry cup method.

b.)	Aggregate for traffic surface coating shall be suitably graded, fine trap-rock passing a #20 	mesh sieve and retained on a #40 mesh sieve.

c.)	Fabric used as reinforcement for waterproof membrane or protection coat (as applicable) shall be 7-1/2 oz. woven polypropylene fabric.

# 2.02	PROPERTIES

A.	Colors:  As indicated, or if not otherwise indicated, as selected by Architect from manufacturer's standard colors.

B.	Physical Properties:

Provide a waterproof membrane system that meets or exceeds the listed minimum physical property requirements when tested according to the referenced standard test methods in parentheses.

Bond Shear Strength (ASTM 482)		Dry 77 p.s.i.

Wet 62 p.s.i.

Tensile Strength (CTI SE S763)			Dry 46 p.s.i.

Wet 50 p.s.i.

Breaking Strength (ASTM D751)		265 p.s.i.

Elongation (ASTM D751)			50.5%

Bacteria and Fungus (ASTM G22)		No Growth / No Water

Resistance					Penetration

Hydrostatic Pressure (ASTM D751)		240 p.s.i.

Resistance

Ozone Resistance (ASTM D1149)		No cracking, orating, or water

(72 hrs @ 100ppm 90 Degrees F)			Penetration

Dimensional Stability (ASTM D1204)		<0.5%

Indentation Resistance (FMA 4900.1)		No Water Penetration

Puncture Resistance (FMA 4900.1)		No Water Penetration

System Performance (ASTM627)		Complies

# PART 3.00 - EXECUTION

301	CONTRACTOR QUALIFICATIONS

A.	Fracture resistant membrane system shall be installed in strict accordance with the manufacturer's recommendations by a contractor trained and approved by the materials manufacturer and has a minimum five years experience in the application of similar materials.

# 3.02	INSPECTION

A.	Examine the areas and conditions where the waterproof neoprene composition fracture Resistant waterproof membrane system is to be installed and notify the Architect of conditions detrimental to the proper and timely completion of the work.  Do not proceed with the work until unsatisfactory conditions have been corrected by the Contractor in a manner acceptable to the Architect.

B.	Evaluate level of moisture in the substrate to determine that moisture levels are acceptable for application of specified waterproof deck covering system.

303	PREPARATION

- Perform preparation and cleaning procedures according to waterproof membrane manufacturer's instructions for particular substrate conditions involved, and as specified.  Provide clean, dry and neutral substrate for application of waterproof deck covering.

B.	Materials:  Mix aqueous emulsions and aggregate when required as per manufacturer's instructions. Prepare materials according to waterproof membrane system manufacturer's instructions.

# 3.04	FIELD CONDITIONS

A.	Fracture Resistant membrane system shall not be applied during either freezing or inclement weather, or when such weather can logically be expected.

# 3.05	APPLICATION

A.	General:  Apply each component of waterproof neoprene composition fracture Resistant waterproof membrane system according to manufacturer's directions to produce a uniform monolithic surface of thickness indicated.

- Apply Dex-O-Tex A-81 Underlayment into 2.5 expanded metal lath over the entire surface to be coated. Incorporate any slope for drainage required.

- Apply aqueous polyacyralate Co-Polymer primer coat over entire area. Allow to cure a minimum of two hours before proceeding.

D.	Apply reinforced membrane at all vertical junctures. Embed polypropylene fabric into neoprene membrane liquid.

E.	Apply two or three coats of aqueous neoprene rubber waterproof membrane as required to achieve a minimum thickness of 25 mils DFT to entire area to be coated.

F.	Trowel apply two coats of polyacyralate Co-Polymer and fine aggregate composition with reinforcing R.P. fabric to achieve smooth,  protection coat.

3.04      CURING, PROTECTION AND CLEANING

A.	Cure waterproof neoprene composition fracture Resistant waterproof membrane system materials according to manufacturer's directions, taking care to prevent contamination during application stages and before completing curing process.  Close application area for a minimum of 24 hours.

# END OF SECTION

DEX-O-TEX PRODUCT LINE 			3000 E. Harcourt Street		140 Valley Road

Crossfield Products Corp.			Rancho Dominguez, CA 90221		Roselle Park, NJ 07204

www.dexotex.com				Tel: (310) 886-9100			Tel: (908) 245-2800

Fax: (310) 886-9119			Fax: (908) 245-2583