# SECTION 09400

# POLYACRYLATE MATRIX TERRAZZO

# Dex-O-Tex Spectrum Terrazzo

# PART 1.00 - GENERAL

# 1.01	GENERAL REQUIREMENTS

A.	Work of this Section as shown or specified shall be in accordance with the requirements of the Contract Documents.

# 1.02	WORK INCLUDED

A.	Work of this Section includes all labor, materials, equipment and services necessary to complete polyacrylate matrix terrazzo flooring and integral coved base as selected on drawings and/or specified herein.

# 1.03	RELATED WORK

A.	Concrete - Section 03300 (Note to specifier:  Concrete should be either water cured or cured using sodium silicate curing compounds only.  Other types of curing compounds are generally not acceptable.  Concrete should be cured for a minimum of 28 days.  On grade floors should have functioning vapor retarder beneath slab.)

B.	Floor drains - Division 15.  (Note to Specifier:  Floor drains, clean-outs etc. should be of the floor-flange type as manufactured for use with composition floors by most major drain manufacturers.)

# 1.04	SUBMITTALS

A.	General:  Submit the following in accordance with Conditions of Contract and Division 1 Specification Sections.

B.	Product Data:  Submit manufacturer's technical data application instructions and general recommendations for polyacrylate matrix terrazzo flooring specified herein.

C.	LEED Submittals:

1.  	Product Data for Credit MR 4.1 and Credit MR 4.2:  For products having recycled content, submit documentation indicating percentages by weight of postconsumer and preconsumer recycled content.

a.   	Include statement indicating costs for each product having recycled content.

b.	Include LEED Product Information Form for LEED Credits MR 4.1 and 4.2.

2.	Product Data for Credit EQ 4.2:  For field applied, interior, paints coatings and primers, include printed statement of VOC content indicating compliance with Credit requirements.

a.	Include LEED Product Information Form for LEED Credit EQ 4.2.

3.	Provide additional documentation for products as required to achieve each Credit(s).

D.	Samples for initial selection purposes.

1.  Submit 2-1/2" x 4" samples in color combination as selected.

E.	Material certificates signed by manufacturer certifying that polyacrylate matrix terrazzo flooring complies with requirements specified herein.

F.	Maintenance Instructions:  Submit manufacturer's written instructions for recommended maintenance practices.

# 1.05	QUALITY ASSURANCE

A.	Installer Qualifications:  Engage an experienced installer or applicator who has specialized in      installing polyacrylate terrazzo flooring types similar to that required for this Project and who is acceptable to manufacturer of primary materials.

B.	Single-Source Responsibility:  Obtain polyacrylate matrix component of terrazzo flooring materials including primers, resins, cements and finish or sealing coats from a single manufacturer.  Obtain marble chip aggregates and metal dividing strips from primary manufacturers of those products.

# 1.06	DELIVERY, STORAGE AND HANDLING

A.	Deliver materials in original packages and containers with seals unbroken and bearing manufacturer's labels containing brand name and directions for storage and mixing with other components.

B.	Store materials to comply with manufacturer's directions to prevent deterioration from moisture, heat, cold, direct sunlight or other detrimental effects.

# 1.07	PROJECT CONDITIONS

A.	Environmental Conditions:  Comply with polyacrylate matrix terrazzo manufacturer's directions for maintenance of ambient and substrate temperature moisture, humidity, ventilation and other conditions required to execute and protect work.

B.	Lighting:  Permanent lighting will be in place and working before installing polyacrylate matrix terrazzo flooring.

# PART 2:00 - PRODUCTS

# 2.01	MATERIALS

A.	Polyacrylate matrix terrazzo shall be Dex-O-Tex Spectrum Terrazzo as manufactured by Crossfield Products Corp. in Rancho Dominguez, California and Roselle Park, New Jersey.

# 2.02	PROPERTIES

A.	Colors:  As indicated, or if not otherwise indicated, as selected by Architect from manufacturer's standard matrix colors with marble chips as regionally available.

B.	Physical Properties:  Provide flooring system that meets or exceeds the listed minimum physical property requirements using specified polyacrylate matrix incorporating marble aggregate as per manufacturer's mix recommendations when tested according to the referenced standard test method in parentheses.

Compressive Strength (ASTM C109)	4107 psi.

Impact Resistance (MIL-PRF-3134 Para. 4.7.3)	.02" Indentation

No loosening or cracking

Indentation Resistance	1.05%

(MIL-PRF-3134   Para. 4.7.4.2.1)

Adhesion (MIL-PRF-3134, Para 4.7.14)	>200 psi

Resistance to Elevated Temperatures	No slip, flow or softening

(MIL-PRF-3134, Para. 4.7.5.1)

Tensile Strength (ASTM C190)	797 psi.

Flammability (ASTM E84)	Flame Spread 0

Smoke Density 3

# 2.03	SUPPLEMENTAL MATERIALS

A.	Waterproofing Membrane:  Type recommended or produced by manufacturer of polyacrylate matrix composition flooring system for type of service and floor condition indicated.  (Note to Specifier:  The use of waterproof membrane is optional and is generally confined to suspended floors and in rooms having floor drains and subject to very wet spillage and service.  All areas requiring membrane treatment should be clearly shown on plans and finish schedules.)

B.	Dividing Strips:  Type as manufactured for use with thin-set polyacrylate matrix terrazzo.  (Note to Specifier:  Typical dividing strip is white alloy of zinc in gauge 18, 16, or 14).

# PART 3.00 - EXECUTION

# 3.01	INSPECTION

A.	Examine the areas and conditions where polyacrylate matrix terrazzo flooring is to be installed and notify the Architect of conditions detrimental to the proper and timely completion of the work.  Do not proceed with the work until unsatisfactory conditions have been corrected by the Contractor in a manner acceptable to the Architect.

# 3.02   PREPARATION

A.	Substrate:  Perform preparation and cleaning procedures according to flooring manufacturer's instructions for particular substrate conditions involved, and as specified.  Provide clean, dry, and neutral substrate for flooring application.

B.	Concrete Surfaces:  Shot-blast, acid etch or power scarify as required to obtain optimum bond of flooring to concrete.  Remove sufficient material to provide a sound surface, free of laitance, glaze, efflorescence, and any bond-inhibiting curing compounds or form release agents.  Remove grease, oil, and other penetrating contaminates.  Repair damaged and deteriorated concrete to acceptable condition.  Leave surface free of dust, dirt, laitance, and efflorescence.

C.	Materials:  Mix polyacrylate matrix flooring components when required, and prepare materials according to flooring system manufacturer's instructions.

# 3.03   APPLICATION

A.	General:  Apply each component of polyacrylate matrix flooring system according to manufacturer's directions to produce a uniform monolithic flooring surface of thickness indicated.

B.	Bond Coat:  Apply neoprene composition bond coat over prepared substrate at manufacturer's recommended spreading rate.

C.	Divider Strips:  Set divider strips as indicated on plans.

D.	Body Coat:  Over bond coat surface trowel apply polyacrylate matrix terrazzo to thickness of ___. (Note to Specifier:  Polyacrylate matrix terrazzo is typically applied in either 1/4", 3/8" or 1/2" thickness.  Specification of 3/8" or 1/2" thickness provides floor which helps fair off undulations in concrete surfaces and permits incorporation of larger sized marble chips.)

E.	Grinding:  Grind floor using terrazzo grinding machines, mounting progressively finer grit stones to achieve flat surface with uniform exposure of marble chips.

F.	Grouting and Finish Grind:  Grout floor with polyacrylate resin and finish grind to remove grout.

G.	Sealing Coats:  Apply sealing coats of type recommended by manufacturer to produce finish matching approved samples.  Finished floor shall be ___ thick.) Note to Specifier:  Indicate desired thickness)

# 3.04	CURING PROTECTION AND CLEANING

A.	Cure polyacrylate matrix terrazzo flooring materials according to manufacturer's directions taking care to prevent contamination during application stages and before completing curing process.  Close application area for a minimum of 24 hours.

# END OF SECTION

DEX-O-TEX PRODUCT LINE			3000 E. Harcourt Street		140 Valley Road

Crossfield Products Corp.			Rancho Dominguez, CA 90221		Roselle Park, NJ 07204

www.dexotex.com				Tel: (310) 886-9100			Tel: (908) 245-2800

Fax: (310) 886-9119			Fax: (908) 245-2583