SECTION 07550

MULTI-LAYERED WATERPROOF MECHANICAL EQUIPMENT ROOM FLOOR SURFACING

Dex-O-Tex M-E Flooring

PART 1.00 - GENERAL

1.01	GENERAL REQUIREMENTS

A.	Work of this Section, as shown or specified, shall be in accordance with the requirements of the Contract Documents.

1.02	WORK INCLUDED

A.	Work of this Section includes all labor, materials, equipment, accessories and services necessary to complete the multi-layered troweled waterproof mechanical equipment room floor surfacing and vertical flashing as scheduled on the drawings and/or specified herein.

1.03	RELATED WORK

A.	Concrete - Section 03300.

(Note to Specifier:  A fluid applied film forming curing compound complying with ASTM C309 or ASTM C1315 should be applied to the concrete to facilitate proper curing of the concrete substrate. Other types of curing compounds are generally not acceptable.  Concrete should be cured for a minimum of 28 days.  On grade floors should have functioning vapor retarder beneath slab.)

B.	Floor drains - Division 15.

(Note to Specifier:  Floor drains, clean-outs, etc. should be of the "floor-flange" type as manufactured for use with waterproof floors by most major drain manufacturers.

1.04	SUBMITTALS

A.	General:  Submit the following in accordance with Conditions of Contract and Division 1 Specification Sections.

B.	Product Data:  Submit manufacturer's technical data, application instructions and general recommendations for the multi-layered troweled waterproof flooring surfacing specified herein.

C.	LEED Submittals:

1.  	Product Data for Credit MR 4.1 and Credit MR 4.2:  For products having recycled content, submit documentation indicating percentages by weight of postconsumer and preconsumer recycled content.

a.   	Include statement indicating costs for each product having recycled content.

b.	Include LEED Product Information Form for LEED Credits MR 4.1 and 4.2.

2.	Product Data for Credit EQ 4.2:  For field applied, interior, paints coatings and primers, include printed statement of VOC content indicating compliance with Credit requirements.

a.	Include LEED Product Information Form for LEED Credit EQ 4.2.

3.	Provide additional documentation for products as required to achieve each Credit(s).

D.	Samples for initial selection purposes in form of manufacturer's color charts showing full range of colors and finishes available.

1.	Submit 2-1/2" x 4" samples in color (red or gray) the selection shall be designated by the Architect.

E.	Samples for Verification: For each multi-layered troweled waterproof floor surfacing system or color specified, Provide 2 each, 6 inches (150mm) square samples in the selected color and texture, applied to a ridged backing by the installing contractor for this project.

F.	Material certificates signed by manufacturer certifying that the multi-layered troweled waterproof flooring surfacing supplied for this complies with requirement specified herein.

- Maintenance Instructions:  Submit manufacturer’s written instructions for recommended maintenance practices.

- Contractor Certification: Submit a letter from the primary materials manufacturer certifying that the installing contractor has been properly trained in the application of the materials being installed, and is acceptable to the materials manufacturer.

- Engage an installer who employs only persons trained and qualified for accomplishing preparation and installation of the multi-layered troweled waterproof flooring surfacing systems specified, including any sub-contractors performing work on the project.

- Engage an installer who is certified in writing by the multi-layered troweled waterproof flooring surfacing manufacturer as a factory trained applicator qualified to apply the specified resinous flooring system.

1.05     QUALITY ASSURANCE

- Installer Qualifications:  Engage an experienced Installer or applicator who has specialized in installing waterproof flooring system types similar to that required for this Project. The waterproof flooring system installation contractor shall have a minimum of five year experience for installation in the installation of similar materials and acceptable to materials manufacturer.

B.	Acceptable Materials Manufacturers: Manufacturer shall certify that they are the primary formulator of the materials used in the completion of the work as specified herein. The materials manufacturer shall have a minimum 10 year experience in producing waterproof flooring system materials.  They shall also be a certified ISO 9001 Quality Control manufacture

C.	Single-Source Responsibility:  Obtain multi-layered troweled waterproof flooring surfacing materials, including primers, resins, hardening agents, binders, aggregate blends and finish or sealing coats from a single manufacturer.  Provide secondary materials, including patching and fill materials, joint sealant, accessory items, and repair materials from a source recommended by the manufacturer of the primary materials.

D.	Qualified Materials: Request for material approvals for any product other than the specified products must be submitted to the architect two weeks prior to the bid, including complete application specification, physical characteristics, and chemical resistance data. Any request after this date will not be accepted.  Failure of performance requires immediate removal and replacement of unapproved substituted material with those originally specified at no cost to the owner, architect, construction manager, or general contractor.

E.	Mockups: Apply mockups to verify selections made under sample submittals and to demonstrate aesthetic effects and set the standard of quality for materials and installation.

- Apply all components of the specified multi-layered troweled waterproof floor surfacing system at the specified thickness and finished in the texture and color as selected. Apply a minimum 100 square feet area to simulate the actual installation characteristics. Include areas that demonstrate the finished cove base, joint detailing, terminations or any other special conditions.

- Simulate finished lighting conditions for Architects review of mockups.

- Approved mockups may become part of the completed work if undisturbed at the time of substantial completion.

F.	Inspection of the Work: A SSPC certified CCI concrete coating QA inspector must provide a project inspection plan, perform any specified inspections and verify that the work performed by the contractor meets all of the project specification requirements.

1.06    	DELIVERY, STORAGE AND HANDLING

A.	Deliver materials in original packages and containers with unbroken seals and bearing manufacturer's labels containing brand name, date of manufacture, manufacture lot number and directions for storage and mixing with other components.

B.	Store materials to comply with manufacturer's directions to prevent deterioration from moisture, heat, cold, direct sunlight, or other detrimental effects.

1.07    PROJECT CONDITIONS

A.	Environmental Conditions:  Comply with multi-layered troweled waterproof floor surfacing system manufacturer's directions for maintenance of ambient and substrate temperature,         moisture, humidity, ventilation and other conditions required to execute and protect work.

- Lighting:  Permanent lighting will be in place and working before installing multi-layered troweled waterproof floor surfacing system.

- Moisture Vapor Emission Rates: Perform Calcium Chloride test in conformance to ASTM F1869 or in situ relative humidity test conforming to ASTM F2170 to determine moisture vapor emission rates or in situ relative humidity in substrate prior to application of any component of the flooring system. Do not install flooring over substrate with moisture vapor emission rates in excess of 3 lbs. per 24 hour period over a 1000 square foot area or with a relative humidity in excess of 78%. Notify the Architect and Project Administrator immediately if MVER or rh levels exceed these rates.

PART 2.00 – PRODUCTS

2.01	MATERIALS

- Multi-layered troweled waterproof mechanical equipment room floor surfacing system shall be Dex-O-Tex M-E Flooring as manufactured by Crossfield Products Corp. in Rancho Dominguez, California and Roselle Park, New Jersey.

- Multi-layered trowel applied waterproof flooring surfacing system shall be composed of a primer bondcoat, waterproof membrane, traffic surfacing and finish coats, and shall conform to the following standards:

1.	Traffic surface binder and all rubber emulsions shall be compounded with an aqueous synthetic rubber liquid containing no hydrocarbon solvents.

2.	Aggregate for traffic surface coating shall be suitably graded mineral aggregate passing a #20 mesh sieve and retained on a #80 mesh sieve.

3.	Fabric used as reinforcement for waterproof base and floor shall be 7 ½ oz. woven polypropylene fabric.

4.	Final Finish dressing shall be a single component, water-phase acrylic latex emulsion material, pigmented and of a consistence suitable for roller application.

  - PROPERTIES

- Colors: As indicated or if not otherwise indicated, as selected by Architect from manufacturer’s standard colors.

B.	Physical Properties:  Provide a flooring system that meet or exceed the listed minimum physical property requirements when tested according to the referenced standard test method in parentheses.

Waterproofness (Smith Emery Laboratories Test Procedure)

Sample 18” diam. Subjected to 50 lbs per inch water pressure

for 60 mins.  Test for amount of water forced through in grams.

Tensile Strength & Elongation (ASTM D1117):

Elongation Dry	29.0%

Breakload Dry	106 lbs. per inch

Elongation Wet	31.0%

Breakload Wet	67 lbs. per inch

Strip Adhesion

(Strip adhesion measured in per linear inch force

required to pull up membrane)	19.2 lbs. per inch

Indentation Characteristics (MIL-D-3134, Para. 4.7.3)

(Steadily Applied Load)  (2000 lbs. on 1” steel

ram imposed for 30 minutes)	< 5%

Indentation Characteristics (MIL-D-3134, Para. 4.7.3)

(Impacted Load 2 lb. Steel ball dropped

from 8 foot height)	No cracking or loosening

Resistance to Elevated Temperature

(MIL-D-3134, Para 4.7.5.1)	No flow or slip

Skid Resistance (Coefficient of Friction)	Varies depending upon surface

texture selected.

PART 3.00 - EXECUTION

3.01	INSPECTION

A.	Examine the areas and conditions where the multi-layered troweled waterproof flooring surfacing is to be installed and notify the Architect of conditions detrimental to the proper and timely completion of the work.  Do not proceed with the work until unsatisfactory conditions have been corrected by the Contractor in a manner acceptable to the Architect.

B.	Job Site Pre-Installation Survey

1.	Perform moisture testing in accordance with ASTM F1869, ASTM F2170 or ASTM E1907.  Verify and document result in accordance with the specification. If the MVER exceeds 3 lbs. or the relative humidity (RH) of the substrate is greater than 78%, apply Dex-O-Tex VaporControl Primer 200 as per manufacturer’s application specification before proceeding.

2.	Inspect Substrate to verify proper preparation before applying any materials.

3.	Measure and record ambient temperature and humidity, surface temperature and the temperature of the material being used at the start of work, mid-day and at the commencement of work each day. Do not proceed with the application if the conditions are outside the recommended parameters Inspect materials to be used.  Verify material is the proper material and all components and sizes are correct. Inspect all containers and verify a proper factory seal with no signs of damage or leakage. Premix Liquid materials into a smooth homogenous blend before uses.

3.02	PREPARATION

- Substrate:  Perform preparation and cleaning procedures according to waterproof floor surfacing manufacturer's instructions for particular substrate conditions involved, and as specified.  Prepare in accordance with SSPC SP 13/NACE No. 6.

- Concrete Surfaces:  Shot-blast, or power grind as required to obtain optimum bond of flooring to concrete.  Remove sufficient material to provide a sound surface free of laitance, glaze, efflorescence and any bond-inhibiting curing compounds or form release agents.  Remove grease, oil and other penetrating contaminates.  Prepare substrate in accordance with SSPC SP 13/ NACE No.6. Repair damaged and deteriorated concrete to acceptable condition.  Leave surface free of dust, dirt, laitance, and efflorescence. Perform surface cleanliness test in conformance with ISO 8502.

- Materials:  Mix resin hardener aqueous emulsions and aggregate as required and prepare materials according to flooring system manufacturer's instructions.

3.03	APPLICATION

A.	General:  Apply each component of multi-layered troweled waterproof flooring surfacing system according to manufacturer's directions to produce a uniform monolithic surface of thickness indicated.

- Environmental Check Points: Measure and record ambient temperature, relative humidity, dew point, surface temperature, and material temperatures at the beginning of work, mid-day, and at the end of work each day work is performed on the project. Include this information with the joint installer manufactures guarantee as part of the project close out documents.

- Apply synthetic rubber waterproof membrane solution at all vertical junctures.  Embed polypropylene fabric into membrane liquid.

- Apply synthetic rubber waterproof membrane solution with polypropylene fabric reinforcement to entire area to be coated.  Overlap all seams a minimum of 2 inches.

- Trowel apply elasticized resin emulsion and aggregate composition traffic surfacing over all surfaces previously covered with waterproof membrane at nominal 1/8” finish thickness as specified..  Sand surface to remove trowel marks or small surface imperfections.

- Roller apply two coats of final finish dressing to a uniform finish. : (Optional) NOTE TO SPECIFIER: Various optional top coats are available for specific performance criteria or esthetic requirements. Please consult Crossfield Products Corp. for assistance in selection of optional top coats.

- Finished waterproof mechanical equipment room floor surfacing shall be a nominal 3/16 inch thick, uniform in color and texture.

- Cove Base:  Apply cove base mix to wall surfaces at locations shown to form cove base height of 4 inches unless otherwise indicated.  Follow manufacturer's printed instructions and details including taping, mixing, troweling, and sanding, of cove base.

3.04    	CURING, PROTECTION AND CLEANING

- Cure multi-layered troweled waterproof flooring surface materials according to manufacturer's directions, taking care to prevent contamination during application stages and before completing curing process.  Close application area for a minimum of 24 hours.

# END OF SECTION

DEX-O-TEX PRODUCT LINE	3000 E. Harcourt Street	140 Valley Road

Crossfield Products Corp.	Rancho Dominguez, CA 90221	Roselle Park, NJ 07204

www.dexotex.com	Tel: (310) 886-9100	Tel: (908) 245-2800

Fax: (310) 886-9119	Fax: (908) 245-2583